## Slide 1: CHEM-E5115 Microfabrication Homework 3
Lingju Meng
Mar. 2023

## Slide 2: HW3 Q1
If 250-minute wet oxidation results in 1 µm thick oxide, how long will it take to grow 5 µm oxide under same conditions?
How long will it take to grow 200 nm thick oxide? Hint: Use the parabolic assumption, figure 13.3.

## Slide 3: HW3 Q2
Make a comparison of thermal oxide versus CVD oxide. Compare film processing, quality, thicknesses, applications… side by side.

## Slide 4: HW3 Q3
Draw where 0.5 µm thick thermal oxide will grow in the structure shown below. The figure is DRAWN TO SCALE !! Trench width is 1 µm and epilayer thickness 1.5 µm and so on. Detail drawing needed; no points for hasty sketches. (Hint: scan your drawing)
Describe other phenomena that will happen during the oxidation process. (Hint: crystal and dopants)

## Slide 5: HW3 Q4
Design a fabrication process for this device. Process flow is a numbered list like:
Choose p-type silicon wafer
Deposit …
XXX
YYY
ZZZ
It must be strictly chronological: think of it as an algorithm that is executed by somebody else in the cleanroom.
Propose deposition methods, film thicknesses and lithographic linewidths.
This is an ‘open’ question. Any reasonable thickness and linewidths will be considered correct. Better to have references for the values. Hint: it might be a solar cell.