## Slide 1
Surface MEMS
(based on chapter 29)
with audioclips
sami.franssila@aalto.fi

## Slide 2: Generic structure
Sacrificial material
Structural material
Substrate material
Structural material
Substrate material
anchor
anchor

## Slide 3: Applications

## Slide 4: Isotropic etching
Proceeds as a spherical wave
Undercuts structures (proceeds under mask)
Most wet etching processes are isotropic
e.g. HF etching of oxide, H3PO4 etching of Al

## Slide 5: Isotropy: good and bad
If you want closely spaced lines (as in comb-drive capacitor), undercutting is bad, but if...

## Slide 6: Single-mask mechanical amplifier
P. Schmitt and M. Hoffmann, "Engineering a Compliant Mechanical Amplifier for MEMS Sensor Applications," in Journal of Microelectromechanical Systems, vol. 29, no. 2, pp. 214-227, April 2020.

## Slide 7
Single mask vs. two mask cantilever
Single mask process
Two mask process
mask #2
mask #1
mask
Litho 1
Etch anchor hole in sacrificial layer, strip resist
Deposit structural layer
Litho 2
Etch structural layer, strip resist
Etch sacrificial layer
Etch structural layer with resist mask,
strip resist
Etch sacrificial layer

## Slide 8
Material pairs & etchants
Structural film Sacrificial film Sacrificial etch(es)
polysilicon oxide HF, HF vapor
silicon nitride oxide HF
silicon nitride Al NaOH, H3PO4
nickel Cu HCl
nickel resist oxygen plasma
aluminum resist oxygen plasma
gold Cu HCl
gold resist oxygen plasma
copper resist oxygen plasma
Parylene resist acetone, other solvents
SU-8 Cu HCl
CVD oxide CVD polysilicon SF6 plasma, XeF2 vapor
Deposition >300oC
Must handle 300oC

## Slide 9
HF etching of SiO2 and other materials
Etchant Material
SiO2 TEOS PSG Si3N4 Al Mo
HF (49%) 1763 3969 4778 15 38 0.15
BHF 133 107 1024 1 3 0.5
1:10 HF 48 157 922 1.5 320 0.15
Etch rates in nm/min
These are CVD oxides
Thermal oxide
Thermal oxide properties are always the same, but (PE)CVD oxide properties are strongly deposition process dependent

## Slide 10: Polysilicon
SiH4 (g) ==> Si (s) + 2 H2 (g)
Deposited by CVD at 625oC  true poly
Can be deposited at 575oC  amorphous
Typical thickness 100 nm-2 µm
CMOS gate electrodes
MEMS rotors

## Slide 11: Poly vs. <Si>
Density: same for both 2.3 g/cm3
Young’s modulus: same for both 170 GPa
CTE: same for both 2.5 ppm/K
Thermal conductivity: <Si> 156 W/K*m
poly 32 W/K*m
Carrier mobility: <Si> 100 cm2/Vs
poly 10 cm2/Vs

## Slide 12: Compressive stresses in film
buckling
Buckling depends on:
Material (E, υ)
Bridge span (L)
Bridge thickness (t)
Critical buckling stress

## Slide 13: Desired state of affairs in most cases: structural layer is flat after release
This is achieved by (small) tensile stress

## Slide 14: Tensile stress issues
Film stays flat.
Film will crack if too high tensile stress.
Defects (e.g. cracks) initiate breakage (aided by high tensile stresses).

## Slide 15
Marc Madou

## Slide 16
Perforation to release large area structures

## Slide 17
Thermally excited resonator
CVD oxide deposition
Poly deposition
Lithography piezoresistor
Implant piezo & strip
Clean
Anneal implant damage
Au evaporation
Litho for heater
Au heater etch & strip
Litho for poly hole
Poly etch & strip
Oxide wet etch in HF
Rinse & dry
oxide
poly
Reichenbach, R.B. et al:, IEEE EDL 27 (2006) p. 805

## Slide 18: Lateral-field-excited (LFE) piezoelectric AlN contourmode
Zuo et al.: CMOS oscillator based on contour-mode MEMS resonators, IEEE 2010

## Slide 19: LFE AlN fabrication
(a) AlN sputter deposition on top of Si
wafers
(b) lithography, Pt electrode deposition evaporation, lift-off
(c) AlN lithography and plasma etching using Cl2 and BCl3, continue to etch into Si
(d) structure release by Si dry etching in XeF2.
Zuo et al.: CMOS oscillator based on contour-mode MEMS resonators, IEEE 2010

## Slide 20: Microphone
aluminum membrane
N+ diffusion
oxide
0. SSP wafer, low n-doping
Thermal oxide
1st litho for diffusion
Etch oxide & strip resist
Clean
N+ diffusion, heavy doping
Etch all oxide away
CVD oxide deposition
2nd litho: open contact to n+
Etch oxide & strip resist
Aluminum sputtering
3rd litho: holes in Al membra
Etch aluminum & strip resist
Etch oxide, rinse & dry

## Slide 21: Stiction (sticking + friction)
Capillary force of liquid exceeds mechanical strength of the released beam, and the released beam attaches to substrate
Stiction, permanent
correct release

## Slide 22: Stiction prevention
Replace water by something that has lower surface tension, like isopropyl alcohol
Use stronger structure shapes (H, T, I, U beams)
Change structural material
Redesign so that shorter beams needed
Redesign larger gap (not always possible)
Make surfaces rough (opposite of good bonding!)
Use dry release  no drying needed
Use more elaborate drying (more on next slide)

## Slide 23
Alternative drying
SD: Via vapor phase  no surface tension effects
FD: Via solid phase, directly to gas, eliminating liquid phase

## Slide 24: Stiction prevention: plasma release
No liquid, no surface tension, no capillary forces.
Other plasma releases:
SF6 isotropic plasma etching of silicon
NF3, ClF3, also sources of fluorine to etch silicon

## Slide 25: Dry release, but no plasma
XeF2:
etches silicon, silicon nitride and molybdenum.
Selectivity to oxide >1000:1
HF vapor:
etches SiO2.
Of course, CVD oxides still etch faster than thermal oxide.
Aluminum OK. Nitride selectivity 40-600:1, depends on details.
Two different sacrificial layers !

## Slide 26: MEMS switches
(b) Resistive Shunt,
(d) Resistive Series.
K. Srinivasa Rao, Lakshmi Narayana Thalluri; Journal of Biosensors, Biomarkers and Diagnostics
Capacitive Shunt,
(c) Capacitive Series,
Dielectric between metals
Metal-metal contact

## Slide 27
Capacitive shunt switch
Off-state when up.
On-state when pulled down.
Electrodes for actuation voltage
RF signal electrodes

## Slide 28
Electroplated gold switch
Pull down electrode: Cr/Au, 50/250 nm. 1st deposition, sputter
Sacrificial material: 1 µm Cu
Top contact metal: Au, 0.5 µm
Cantilever: Au, 8 µm
2nd deposition, sputter
3rd deposition, electroplating

## Slide 29
Au

## Slide 30
Electroplated gold switch
Pull down electrode: Cr/Au, 50/250 nm. 1st deposition, sputter
Sacrificial material: 1 µm Cu
Top contact metal: Au, 0.5 µm
Cantilever: Au, 8 µm
2nd deposition, sputter
3rd deposition, electroplating

## Slide 31
Electroplated gold switch
Rebeiz, G.M. & J.B. Muldavin: IEEE Microwave Magazine, Dec. 2001, p. 59

## Slide 32: Critical release gap
Sometimes gap height is critical for device operation. These gaps are often ~ 1 µm in size.
Actuation voltage depends on gap height. If gap bad reproducibility  voltage differences in actuation.
Optical path length depends on gap. If gap control bad  no display of colors.

## Slide 33: Non-critical release gap
Gap provides space so that elements can move;
or gap provides thermal isolation. Large: >> 1 µm

## Slide 34
Sideways movement thermal relay
Heater current of electrothermal actuator
Signal current
Electrical isolation between the two currents
Movement due to thermal expansion
Wang, Y. et al: A low-voltage lateral MEMS switch with high RF performance, J.MEMS 13 (2001) pp. 902-911

## Slide 35
Sideways movement thermal relay
Wang, Y. et al: A low-voltage lateral MEMS switch with high RF performance, J.MEMS 13 (2001) pp. 902-911

## Slide 36
Hinged structures (1)

## Slide 37
Hinged structures (2)

## Slide 38
Hinged structures (3)

## Slide 39: µ-mirror array on CMOS
Ljungblad, U. et al: New laser pattern generator for DUV using a spatial light modulator, Microel.Eng. 57–58 (2001) pp. 23–29

## Slide 40: Bulk vs. SOI vs. surface
In surface micromechanics device functionality is in thin films (oxide, nitride, poly, aluminium…).
Structure heights
1-2 µm (= typical sputter & CVD film thicknesses).
Isotropic sacrificial etching must be used.
In bulk micromechanics <Si>
structure heights
380 µm/500 µm
(= thru-wafer)
Etched either by KOH or by DRIE.
Device functionality in SOI device layer
5-50 µm typical device layer thicknesses
Utilizes DRIE to make closely spaced structures like comb-drives.
Aspect ratios e.g. 10:1