## Slide 1: Microfabrication 2019: lab demo process flow

## Slide 2: Lab demo device: Al resistor
Process flow:
Silicon wafer
Thermal oxidation
Aluminum sputtering
Lithography for resistor
Aluminum etching
Resist strip
Electrical measurements
<Si>
SiO2
Al
Cross sectional view
Al
SiO2
Layout/top view

## Slide 3: Resistor test wafer
A large number of test structures for 2-point resistance measurements:
-different widths
-different lengths
-straight and meandering

## Slide 4: Silicon wafer selection
Wafer size: 100 mm
All Aalto Micronova equipment is geared towards 100 mm wafer size.
Some can handle 150 mm but not all.

## Slide 5: Silicon wafer selection: SSP
p+ substrate wafer
p- epitaxial layer
n-type handle wafer
p-type device wafer
SiO2
DSP
SSP
SSP=
Single side polished
DSP = double side polished
Epi-wafer
SOI-wafer

## Slide 6: Wafer orientation
We always use <100> oriented wafers unless otherwise needed,
because:
-cheap and available
-break nicely for SEM

## Slide 7: Silicon wafer: doping
In this work, thermal oxide will completely isolate the electrical functions from the wafer  no special need for certain doping level.

## Slide 8: Wafer cleaning in 3 steps
Name/alias Chemical composition Temp./time
RCA-1 NH4OH:H2O2:H2O (1:1:5) 70-85oC, 10-20 min
SC-1, standard clean;
APM;
ammonia-peroxide mixture
RCA-2 HCl:H2O2:H2O (1:1:6) 70-85oC, 10-20 min
SC-2;
standard clean-2;
HPM, hydrogen chloride-peroxide mixture
DHF (dilute HF) HF:H2O (1:100-1000) room temp., 30 s
(and rinse and dry)

## Slide 9: Cleaning functions
RCA-1:
Removes particles
Removes organics
RCA-2:
Removes metals
DHF: removes native oxide
Other reasons for cleaning:
-eliminates wait time differences
-eliminates previous step effects

## Slide 10: Pre-oxidation cleaning
High temperature  high mobility of impurities  more problems
Thinner oxide  more sensitive to surface quality

## Slide 11: Oxidation furnaces

## Slide 12: Dry oxidation

## Slide 13: Wet oxidation: 10000C, 110 min
510 nm thick
(blue-green color).
Why not 580 nm ?
(light orange)
The growth curves are simulations with a simple simulator.

## Slide 14: Oxide thickness
By ellipsometry

## Slide 15: Why not CVD oxide ?
Thermal oxide is better quality.
What does oxide quality entail ?
Uniform (±1%)
Dense
Low interface charge density
Low defect density
High breakdown voltage
Because we can use thermal oxidation !!!!
No material on wafer prevents us from it !

## Slide 16: Why no cleaning before sputtering ?
Wafers coming from 1000oC oxidation furnace are maximally clean.
No cleaning process can improve them.
If there is a long wait between oxidation and sputtering, then it is wise to clean the wafers (with RCA-1).
Sputtering is a room temperature process, impurities not very mobile.

## Slide 17: Sputter

## Slide 18: MRC sputter
Batch machine:
9 wafers in one run
(suitable for any wafer size and shape since wafers simply on a flat chick).
No load lock  have to pump longer to reach base pressure.

## Slide 19: Aluminum sputtering
Standard metallization technique.
Metallization thickness has to be > 100 nm for conductors in order to have low enough resistance.
1 µm is enough for most applications;
5 µm is used in power transistors and solar cells that have large currents.
Different layer thicknesses for different groups.

## Slide 20: Aluminum quality
Resistivity
Stress
Adhesion
Uniformity

## Slide 21: Aluminum microstructure
This will be modified in post deposition steps !

## Slide 22: Stress-temperature

## Slide 23: TCR: temperature coefficient of resistance
Looks nice, linear and reproducible, but it is only
22-63oC !
You will measure up to 450oC.

## Slide 24: Aluminum pros and cons
Al has been used widely in the past and is still used
− Low resistivity (only Ag, Au and Cu lower)
− Ease of deposition (sputtering and evaporation)
− Wet and dry etching
Ohmic contacts to Si
Excellent adhesion to dielectrics
Problems with Al
− Silicon is soluble to Al  shallow junction pitting
• Electromigration=> lower life time
• Hillocks=> shorts between levels

## Slide 25: Al-Si phase diagram
Al
Si
Si is soluble in aluminum and open volume is left behind as silicon atoms migrate into aluminum. Aluminum, on the other hand, will diffuse to fill in the space left by silicon dissolution
Atom % Si

## Slide 26: Lithography: bake & prime
Bake at 120oC for an hour to remove adsorbed water.
Treat with HMDS to make surface hydrophobic.

## Slide 27: Lithography: resist choice
Positive resist AZ5214 is chosen.
Positive resists are:
-common
-developed in water-based solutions
-good enough adhesion
-easily stripped

## Slide 28: Lithography: spinning
3 ml of AZ5214 is spin coated, resulting in 1.4 µm thick film.
What percentage of resist ends up on wafer ?
Final spinning 4000 rpm
(partial drying via evaporation)

## Slide 29: Bake on a hot plate
Ensure that solvent is gone.
Not too much heat, because the photoactive compound is also thermally activated !

## Slide 30: Lithography: alignment
No alignment needed because this is the first pattern.

## Slide 31: Lithography: alignment (2)
If the first pattern is ion implantation or diffusion, nothing visible results on the wafer.
Then, it is customary to start the process by making alignment marks in a separate litho & silicon etch as the very first step.

## Slide 32: Lithography: exposure tool

## Slide 33: Lithography: exposure tool MA-6

## Slide 34: Lithography: soft contact
Soft contact:
-we make rather wide lines, no need to push performance to limit
-better linewidth control than proximity litho

## Slide 35: Development
Optimal time depends on:
-resist thickness
-resist bake
-exposure dose
-developer concentration/age

## Slide 36: Resist profile
Resist profile rather sloped
OK, because we are not making narrow lines
Does not matter so much in wet etching, because resist:aluminum selectivity in H3PO4 is very high (>>100:1)

## Slide 37: Hard bake @ 120oC
Completes the photochemical reactions
Improves adhesion
Tradeoff with ramp rate and overshoot.
If a batch of wafers is done, oven bake may be a good choice.

## Slide 38: Wet etching aluminum
H3PO4 -based etch
Heated to 50oC to speed up the process
Plasma etching not used because:
-it is difficult and expensive
-wide linewidth  no need to vertical profile

## Slide 39: Resist strip
Acetone is quick and dirty
Works OK because positive resist which has not been put to aggressive environment
Oxygen plasma or ozone would be needed if Cl2 plasma etching of aluminum was used.

## Slide 40: Aluminum thickness
Profilometer Dektak
Mechanical needle is scanned over steps.
As seen in the figure, needle shape does not really allow PROFILE measurement, but only step height.

## Slide 41: Electrical measurements
Al wire resistances measured (Multimeters)
Calculate resistivity
Annealing on a hot plate up to 200oC, measure during coolo-down, determine TCR
Anneal at 450oC for 20 min
Remeasure wire resistances at 20oC
Write a personal report
(return by March 31st, 10 pm)
Instructions in the lab data sheet