## Slide 1: Scaling
sami.franssila@aalto.fi

## Slide 2: Wafer size scaling
525 µm
625 µm
725 µm
775 µm
?? 925 µm

## Slide 3
Wafer specs scaling for CMOS
Wafer size 100 125 150 200 300 mm
Thickness 525 625 675 725 775 µm
TTV 3 3 2 1.5 1 µm
Warp 20-30 18-35 20-30 10-30 10-20 µm
Flatness <3 <2 <1 0.5-1 0.5-0.8 µm
Oxygen 20 17 15 14 12 pmma
OISF 100-200 100 <10 none none cm-2
Particles 10 10 5-10 10-100 50-100 #/wafer
Particle size 0.3 0.3 0.3 0.16 0.12 µm
Metals 1012 1011 1011 5*1010 109 atoms/cm2

## Slide 4: Wafer sizes (2001 prediction)
Doering, R. & Y. Nishi: Limits of integrated circuit manufacturing, Proc. IEEE Vol. 89 (2001) p. 375

## Slide 5: Wafer sizes (2013 prediction)
https://www.extremetech.com/extreme/163372-atom-everywhere-intel-breaks-ground-on-first-450mm-fab
2013

## Slide 6: Fab cost scaling
1957 0.2 M$
1967 2.5 M$
1977 10 M$
1987 100 M$
1997 1000 M$
2007 3000 M$
2017 6000 M$
Economist April 6, 2018:
TSMC new fab will cost $20B

## Slide 7: Fab size scaling
Year Wafer size LW WPM*
1970 3” 10 µm 1000
1980 100 mm 2 µm 5000
1990 150 mm 0.8 µm 10000
2000 200 mm 0.18 µm 20000
2010 300 mm 32 nm 50000
2020 300 mm 11 nm 70000
* Wafer starts per month

## Slide 8: Making 450 mm etcher
Maximum throughput of an etch tool is governed by two basic factors:
  1) wafer load/unload time
  2) etch time.
With good engineering wafer throughput is independent of wafer size, so that chip throughput improves as the wafer size increases.
Chris Mack: http://www.lithoguru.com/scientist/essays/why450.html

## Slide 9: Making 450 mm etcher (2)
But “good engineering” is not free, and it takes work to keep the etch uniformity the same for a larger wafer.
The larger etch tools also cost more money to make. But if the tool cost does not increase as fast as the wafer area, the result is a lower cost per chip.
This is the goal, and the reason why we pursue larger wafer sizes.
Chris Mack: http://www.lithoguru.com/scientist/essays/why450.html

## Slide 10: Cost analysis of 450 mm etcher
Wafer diameter increase of 1.5X compared with 300 mm
Wafer area increases by factor of 2.25
Because edge die effect it is possible for the number of good chips to increase at a slightly higher amount, maybe up to a factor of 2.4.
If the cost of the etcher, the amount of fab floor space, and the per-wafer cost of process chemicals all increase by 30%, the cost per chip will change by 1.3/2.25 = 0.58.
Thus, the etch cost per chip will be 42% lower.

## Slide 11: 450 mm lithography
Reduction stepper litho process time consists of:
  1) wafer load/unload time
  2) Exposure time
The load time can be kept constant as a function of wafer size, but the exposure time increases as the wafer size increases.
And since wafer load/unload time is a very small fraction of the total process time, the result for lithography is a near-constant wafer-area throughput (rather than the constant wafer throughput for etch) as wafer size is changed.
 Proportion of lithography of total costs will increase. Today 50%

## Slide 12: Latest predictions
450mm Officially On Hold…
January 17, 2017
Is 450mm over? Not for good. At some point, technology, market, and the resulting economic changes will inevitability bring the discussion, and likely, the development, back. However, the New York-based, 450mm global consortium, G450C is done.

## Slide 13: Optical projection lithography

Sources of radiation
(UV 365 nm-436 nm,
DUV 193 nm-248 nm,
EUV, X-rays, electrons, ions)
Optical system I
(lenses, mirrors)
Mask (pattern)
Optical system II
(lenses, mirrors)
Numerical aperture NA=sin 
Imaging medium (resist)
Wafer (with patterns)
Wafer stage
(alignment mechanism)

## Slide 14: Projection litho performance

## Slide 15
Table 10.1: Linewidth scaling of CMOS
Wavelength Aperture k factor Linewidth DoF
=436 nm NA=0.38 k1=0.8 1 µm 1.5µm
=365 nm NA=0.48 k1=0.6 0.5 µm 0.8 µm
=248 nm NA=0.60 k1=0.6 0.25 µm 0.35 µm
=248 nm NA=0.65 k1=0.5 0.18 µm 0.30 µm
Because depth of focus (DoF) gets smaller, CMP planarization becomes more important all the time.

## Slide 16: Projection lithography scaling
Lin, MEMS2010

## Slide 17: Reduction stepper: ~100 exposures/wafer
Nikon.com
Compared to proximity litho:
-much slower
-smaller LW possible
-better alignment

## Slide 18: Reduction factor, often 5X
Mask 1 µm minimum linewidth
5X optical reduction 
0.2 µm on wafer
Mask making becomes much easier and more economical.

## Slide 19: Photomask cost scaling
Min LW Cost
3 µm 300 euros
1 µm 500 euros
1 µm 1000 euros, quality checked
Mask LW Wafer LW Cost
1 µm 0.2 µm 2000 euros
0.5 µm 0.1 µm 5000 euros
200 nm 40 nm 20000 euros
100 nm 20 nm 50000 euros
1X litho
5X reduction litho
For a 40 mask microprocessor  mask set costs $2M

## Slide 20: Refresher: etch profiles
Wet etching  isotropic profile
Plasma etching  anisotropic profile

## Slide 21: Wet etched profile: 1 µm thick film
5 µm
3 µm
2 µm
1 µm

## Slide 22: Plasma etched profile: 1 µm film
5 µm
3 µm
2 µm
1 µm

## Slide 23: Wet etched profile: 200 nm film
5 µm
3 µm
2 µm
1 µm

## Slide 24: Plasma etched profile: 200 nm film
5 µm
3 µm
2 µm
1 µm

## Slide 25
CMP Grenoble
Schematic cross section

## Slide 26: Aspect ratio scaling, real SEM
Actually, aspect ratio (height:width)
does NOT scale;
it has remained more or less 1:1 for decades.
IBM

## Slide 27: 8-level IC metallization

## Slide 28: Comparison of Cu-lines
How would you make the following copper lines ?
50 nm wide, 50 nm thick, perfectly vertical
50 nm wide, 50 nm thick, so-and-so profile
2 µm wide, 10 µm thick, perfectly vertical
10 µm wide, 100 nm thick, so-and-so profile

## Slide 29: 50 nm wide, 50 nm thick
Lithography:
either electron beam or advanced optical litho
If vertical profile needed: damascene.
Litho, etch oxide, sputter seed layer, electroplate, polish
CMP

## Slide 30: 50 nm wide, 50 nm thick
Why not ?
Copper sputter
Lithography
RIE
RIE + strip

## Slide 31: 50 nm wide, 50 nm thick
How about this ?
Copper sputter
Lithography
Ion beam etching
IBE + strip

## Slide 32: 50 nm wide, 50 nm thick
If less well defined profile accpetable: lift-off
Two resist:
LOR (lift-off resist) has faster develop rate.

## Slide 33: Why lift-off sucks ?
Metal pieces floating around in lift-off solution
 low yield, but OK for research.
Requires poor step coverage in deposition
Is done mostly on planar surfaces only
Limits deposition to evaporation (and sputtering)
Requires careful resist profile tailoring

## Slide 34: Why lift-off is good ?
Same process for all metals, no need to find suitable etch liquids or gases
Works for multiple layers of metals
Works for non-etchable metals (Au, Ag, Pt)

## Slide 35: 2 µm wide, 10 µm thick
Seed layer sputtering
Optical lithography
Electroplating
Resist strip
Seed layer etching

## Slide 36: 10 µm wide, 100 nm thick
Sputter 100 nm copper
Lithography
Etch in HCl
Strip resist

## Slide 37: Aspect ratio - nanodevices
This picture is highly schematic.
But if we know that 50 nm lithography is used to make it, we can make some good guesses:
Heater is clearly the smallest structure, i.e. 50 nm.
Aspect ratio 2:1 is realistic, so insulator thickness is 100 nm, and PCM thickness 150 nm.
PCM = Phase Change Memory.
PCM material is either crystalline or amorphous, and its resistance changes dramatically. Thermally programmed.

## Slide 38: Etch selectivity scaling
Case 1: poly:oxide selectivity in gate etching
Case 2: contact hole etch selectivity (oxide:silicon)
Täytyy opettaa oxide thickness and junction depth scaling myös
Leave much of the other etch stuff away, no time

## Slide 40: CMOS linewidth: 5 µm
Polysilicon gate: 500 nm thick
Gate oxide thickness (LW/50) = 100 nm
Etch selectivity poly:oxide = 10:1
Overetch = 50 %
Oxide loss = nm
Oxide loss = % of original thickness

## Slide 41
CMOS linewidth: 5 µm
Polysilicon gate: 500 nm thick
Gate oxide thickness (LW/50) = 100 nm
Etch selectivity poly:oxide = 10:1
Presume: 500 nm/min poly  50 nm/min oxide
Overetch = 50 %  0.5 min oxide etched 
Oxide loss = 25 nm
Oxide loss = 25% of original thickness

## Slide 42: CMOS linewidth: 1 µm
Polysilicon gate: 300 nm thick
Gate oxide thickness (LW/50) = 20 nm
Overetch = 50 %
Oxide loss = same % loss as in above,
Calculate etch selectivity poly:oxide needed to achieve this !

## Slide 43
CMOS linewidth: 1 µm
Polysilicon gate: 300 nm thick
Gate oxide thickness (LW/50) = 20 nm
Overetch = 50 %
Oxide loss = same % loss as in above,
Calculate etch selectivity poly:oxide needed!
Presume 300 nm/min  50% oe is 30 secs
5 nm loss allowed  10 nm/min oxide rate
 30:1 selectivity needed