## Slide 1
Surfaces and Films CHEM-E5150
Surface modification and coating
Jari Koskinen

## Slide 2: Coatings and films terminology
Film or coating is material which is restricted in one dimension
Substrate is solid material supporting the film
Distance from surface/Thickness
  Surface atoms, thin film - Atomic level:
    2 – 5 atom layers on the surface (≈ 0.2 – 0.5 nm)
    over 10 atomic layers (≈ 1 nm) is bulk
  Thin films technically
    1nm – 10 µm
    Needed layer thickness, which is needed to:
      protect substrate
      Wanted functionality of the coating
  Coatings, thick films > 10 µm
Mikko Ritala Thin Films

## Slide 3: Motivations - why thin films?
Interaction of solid material with surrounding often through surface
Modification of surface ➡ material properties
Market of thin films and coatings
  volume about 25 G€ in UK 2005
    about 1% of GNP
  common in all areas of industry
    electronics
    transport
    energy
    building

## Slide 4: Materials Science tetra
Composition
Properties
Processing
Microstructure

## Slide 5: Materials Science and Thin Films tetra
Composition
Properties
Processing
Microstructure
Protection
Transport
Stability
Functionallty
Thin film growth Post processing
Microstructure
Crystallinity/amorphous
Defects
interfaces
Depth distribution
Precipitation
Adsorption

## Slide 6: Processing for surface engineering
Handbook of Physical Vapor Deposition (PVD) Processing – Mattox 2nd edition 2010

## Slide 7
Handbook of Physical Vapor Deposition (PVD) Processing – Mattox 2nd edition 2010

## Slide 8
Handbook of Physical Vapor Deposition (PVD) Processing – Mattox 2nd edition 2010

## Slide 9
Handbook of Physical Vapor Deposition (PVD) Processing – Mattox 2nd edition 2010

## Slide 10
Handbook of Physical Vapor Deposition (PVD) Processing – Mattox 2nd edition 2010

## Slide 11
Handbook of Physical Vapor Deposition (PVD) Processing – Mattox 2nd edition 2010

## Slide 12: Processing for surface engineering
Handbook of Physical Vapor Deposition (PVD) Processing – Mattox 2nd edition 2010

## Slide 13: Coating methods in the next slides
Physical Vapor Deposition including evaporation and sputtering.
Chemical Vapor Deposition and Plasma-Assisted Chemical Vapor Deposition
Electro deposition and Electroless Deposition.
Plasma Spraying

## Slide 14: Coating methods in the next slides
Physical Vapor Deposition including evaporation and sputtering.
Chemical Vapor Deposition and Plasma-Assisted Chemical Vapor Deposition
Electro deposition and Electroless Deposition.
Plasma Spraying

## Slide 15: PVD_Vacuum evaporation
http://tuttle.merc.iastate.edu/ee432/topics/thin_films/evaporation.pdf

## Slide 16: PVD_Vacuum evaporation
http://tuttle.merc.iastate.edu/ee432/topics/thin_films/evaporation.pdf

## Slide 17: PVD_Vacuum evaporation Vapous source
http://tuttle.merc.iastate.edu/ee432/topics/thin_films/evaporation.pdf
Resistive heating
Electron beam heating

## Slide 18: Physical Vapor Deposition PVD. Sputtering

## Slide 19
Plasma is needed to make the gas conductive, and generated ions can then be accelerated to strike the target.
Higher pressures than evaporation: 1-100 mTorr.
Better at depositing alloys and compounds than evaporation.
The plasma contains ≈ equal numbers of positive argon ions and electrons as well as neutral argon atoms. Typically only <0.01% atoms are ionized!
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 20: Sputtering process
Sputtering process can be run in DC or RF mode (insulator must be run in RF mode)
Major process parameters:
  Operation pressure (1-100mTorr)
  Power (few 100W)
  For DC sputtering, voltage -2 to -5kV.
  Additional substrate bias voltage.
  Substrate temperature (20-700oC)
In addition to IC industry, a wide range of industrial products use sputtering: LCD, computer hard drives, hard coatings for tools, metals on plastics.
It is more widely used for industry than evaporator, partly because that, for evaporation:
There are very few things (rate and substrate temperature) one can do to tailor film property.
The step coverage is poor.
It is not suitable for compound or alloy deposition.
Considerable materials are deposited on chamber walls and wasted.
Targets for sputter deposition.
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 21: Advantages/disadvantages
Advantages:
  Able to deposit a wide variety of metals, insulators, alloys and composites.
  Replication of target composition in the deposited films.
  Capable of in-situ cleaning prior to film deposition by reversing the potential on the electrodes .
  Better film quality and step coverage than evaporation.
  This is partly because adatoms are more energetic, and film is ‘densified’ by in-situ ion bombardment, and it is easier to heat up to high T than evaporation that is in vacuum.
  More reproducible deposition control – same deposition rate for same process parameters (not true for evaporation), so easy film thickness control via time.
  Can use large area targets for uniform thickness over large substrates.
  Sufficient target material for many depositions.
  No x-ray damage.
Disadvantages:
  Substrate damage due to ion bombardment or UV generated by plasma.
  Higher pressures 1 –100 mtorr ( < 10-5 torr in evaporation), more contaminations unless using ultra clean gasses and ultra clean targets.
  Deposition rate of some materials quite low.
  Some materials (e.g., organics) degrade due to ionic bombardment.
  Most of the energy incident on the target becomes heat, which must be removed.
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 22: Comparison Sputtering/evaporation
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/ Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 23: Coating methods in the next slides
Physical Vapor Deposition including evaporation and sputtering.
Chemical Vapor Deposition and Plasma-Assisted Chemical Vapor Deposition
Electro deposition and Electroless Deposition.
Plasma Spraying

## Slide 24: CVD
www.ttu.ee › mtx9010 › Korgtehnoloogia_Deposition_methods

## Slide 25
www.ttu.ee › mtx9010 › Korgtehnoloogia_Deposition_methods

## Slide 26: Coating methods in the next slides
Physical Vapor Deposition including evaporation and sputtering.
Chemical Vapor Deposition and Plasma-Assisted Chemical Vapor Deposition
Electro deposition and Electroless Deposition.
Plasma Spraying

## Slide 27: Electro plating
Copper Cathode is reduced
(accepts electrons)
Nickel Anode is oxidized
(gives us electrons)
Ni2+ ions within solution become attracted to Copper cathode
Nick Raymond
www.santarosa.edu › PROJECTS › Electroplating Powerpoint

## Slide 28
Electroless Plating and Electroforming
Electroless Plating
  Chemical Reaction
  More Expensive $$
  Uniform Thickness
Electroforming
  Metal-fabrication
  Metal electrodeposited on a mandrel
Electroplating, Electroless Plating, and Electroforming - UNM ...
www.me.unm.edu › ME260_FALL2005 › Presentation_11_30_05
https://www.vecofrance.fr/en/solutions-techniques

## Slide 29: Conversion Coatings
Anodizing-
  The workpiece is the anode in an electrolytic cell
Coloring-
  Alters color of metals, alloys, and ceramics
  Conversion of surfaces into chemical compounds: oxides, chromates, and phosphates
Electroplating, Electroless Plating, and Electroforming - UNM ...
www.me.unm.edu › ME260_FALL2005 › Presentation_11_30_05

## Slide 30: Coating methods in the next slides
Physical Vapor Deposition including evaporation and sputtering.
Chemical Vapor Deposition and Plasma-Assisted Chemical Vapor Deposition
Electro deposition and Electroless Deposition.
Plasma Spraying

## Slide 31: Thermal spray – coating growth from molten particles
Electroplating, Electroless Plating, and Electroforming - UNM ...
www.me.unm.edu › ME260_FALL2005 › Presentation_11_30_05

## Slide 32: Thermal Spray
Combustion Spraying
  Thermal Wire Spray
  Thermal Metal-Powder Spray
  Plasma Spray

## Slide 33: Thermal spray coating of ball valve
https://www.valve-balls.com/valve-balls/metal-seated-balls.html

## Slide 34: Surface modification
Laser treatment
Ion implantation

## Slide 35: Ion implantation
https://www.hzdr.de/db/Cms?pOid=24316&pNid=0

## Slide 36: Ion implanter
http://blog.bodycote.com/2017/08/02/what-is-ion-implantation/ion-implantation/

## Slide 37: Ion implantation
Low process temperature
Benefits from
  controlled alloying (electrical properties)
  Defects and intersitials (mechanical hardening)
No (or minute) dimensional changes
Expensive

## Slide 38
Laser Treatments
Heating
Melting
Vaporization
Peening
http://www.raymax.com.au/a/157.html

## Slide 39: Laser gladding
http://www.raymax.com.au/a/157.html
https://www.laserline.com/en-int/laser-cladding/