## Slide 1: Surface chemistry
Sami Franssila,
With material from Mikko Ritala,
University of Helsinki

## Slide 2: Surface energy
Seong et al: Dominant mechanisms of the sintering of copper nano-powders, 2016

## Slide 3: Surface tension

## Slide 5: Surface energy of solids

## Slide 6: Estimating surface energy

## Slide 7: Silicon surface energy
Silicon atom surface density, ca. 1015 cm-2, and hydrogen bond energies, 25-40 kJ/mol, which translate to ca. 200-350 mJ/m2.
Surface energies calculated from Si – O bond energies (4.5 eV/bond or 430 kJ/mol) translate to ca. 3000 mJ/m2.
Tong, Q.-Y. & U. Gösele: Semiconductor Wafer Bonding, John Wiley & Sons, 1999

## Slide 8: Surface energy of metals

## Slide 9: Surface energy of metals (2)
Rule of thumb:
-stabilty comes from high surface atom density and high coordination number.

## Slide 10: Surface energy vs. melting point
Bond strength determines both.

## Slide 11: Silicon surface termination
b) Negatively charge H+ repels negatively charged oxygen
Hattori, T. (ed.): Ultraclean surface processing of silicon wafers,
a) Negatively charged oxygen attracts positively charged H+

## Slide 12: Modifying surface chemistry
Methyl-terminated, -CH3
Hydrophobic
Oxygen plasma treatment turns some methyl groups to hydroxyl OH-, groups
 hydrophilic

## Slide 13: SAMs (Self-assembled monolayers)
Either in liquid phase or gas phase deposition.
time

## Slide 14: Silane-SAM

## Slide 15: Self-cleaning mirrors/windows

## Slide 16: Adsorption

## Slide 17: Atoms hitting the surface may:
1. Bounce back
-elastic scattering without energy loss
-inelastic scattering with energy loss
2. Stay on surface
-by weak interaction: physisorption
-by strong interaction: chemisorption
3. Act on surface:
-surface diffusion
-surface reactions
-desorption

## Slide 18: Adsorption concepts

## Slide 19: Coverage Θ

## Slide 20: Adsorbate fate on surface
-move around by surface diffusion
-fragment
-react with substrate
-react with co-adsorbed specie
-react with gas phase specie
-desorb
http://staff.ustc.edu.cn/~bjiangch/research.html
Products may be volatile and desorb; or form film on surface

## Slide 21: Reactive adsorption

## Slide 22: Physisorption

## Slide 23: Xenon atoms physisorbed
“…use of the STM at low temperatures (4 K) to position individual xenon atoms on a single-crystal nickel surface with atomic precision.
The tip of an STM always exerts a finite force on an adsorbate atom. This force contains both Van der Waals and electrostatic contributions. By adjusting the position and the voltage of the tip we may tune both the magnitude and direction of this force. This, taken together with the fact that it generally requires less force to move an atom along a surface than to pull it away from the surface, makes it possible to set these parameters such that the STM tip can pull an atom across a surface while the atom remains bound to the surface.”
The xenon atoms are spaced on a rectangular grid which is four nickel unit cells long horizontally and five unit cells long vertically, corresponding to 14 x 12.5 A.
Eigler & Schweitzer, Nature 1990
Each xenon atom appears as a 1.6-A-high bump on the surface,

## Slide 24: Chemisorption

## Slide 25: Chemisorption vs. physisorption

## Slide 26: Important surface reactions

## Slide 27: Catalysis

## Slide 28: Heterogenous catalysis

## Slide 29: Reaction co-ordinates
https://cnx.org/contents/RTmuIxzM@3.4:bZvv2PMU@4/Catalysis
It might be that homogeneous uncatalyzed reaction is replaced by heterogeneous catalyzed reaction.

## Slide 30: Nobel prize 2007: Gerhard Ertl

## Slide 31: Devil is in the details
Different catalysts

## Slide 32: Pt/C nanoparticle catalyst
Jiang et al: Adv. Funct. Mater. 2020, 30, 2003321
For instance, holes in carbon coating may expose a single Pt-atom; or several  orientation of entering molecule different  different end result

## Slide 33: ALD-coated Pt-catalyst
Cao et al.: Catalysts design and synthesis via selective ALD, JVST A 2018
ALD films <1 nm are discontinuous  gas molecules have access to noble metal catalyst.
But reaction product molecules are too big to enter.

## Slide 34: Stabilization by coating
Biener et al: ALD Functionalized Nanoporous Gold: Thermal Stability, Mechanical Properties, and Catalytic Activity, Nanoletters 2011
Nanoporous gold wants to minimize area, but ALD films prevent this.
In b) nanoscale structures protected by ALD film remain;
In c) unprotected nanoscale structures have coalesced into larger microstructures
b and c –samples both
600oC anneal

## Slide 35: Facet selective deposition
Cao et al.: Catalysts design and synthesis via selective ALD, JVST A 2018
Fe3O4 on Pt, and TiO2 on Au, there is a strong tendency to first nucleate on the egde/low coordinated sites.
The facet selectivity was realized through the intrinsic differences in binding energies of Ce precursor fragments chemisorbed on Pt surfaces.

## Slide 36: Crystal plane dependent etching
54.7o
(100)
(111)
(111)
Some crystal planes etch much faster than others.
In silicon, (100) planes etch 100X faster than (111) planes.

## Slide 37: Bond density at surface

## Slide 38: One layer at a time
https://pmc.polytechnique.fr/spip.php?article580&lang=fr
2 bonds at surface
4 bonds in bulk

## Slide 39: Patterning of catalyst
Cao et al.: Catalysts design and synthesis via selective ALD, JVST A 2018

## Slide 40: Graphene oxide catalyst
Jiang et al: Adv. Funct. Mater. 2020, 30, 2003321
“Co–N4 moieties are surrounded by the
desired configuration of electron-rich oxygen atoms from graphene
oxide substrates.”

## Slide 41: Industrial catalytic processes

## Slide 42: Size scales of catalysis
Chemistry & physics & computational science
Materials science
Chemical engineering
Materials science

## Slide 43: Real surfaces…

## Slide 44: More real surfaces
Belkind & Gershman; Vacuum Technology and Coatng 2008

## Slide 45: Surface functionalization
Chatterjee et al: Core/shell nanoparticles in biomedical applications, 2014