## Slide 1: Surfaces and Films CHEM E5150 Lecture 2A
J Koskinen

## Slide 2: Items:
Ideal surfaces
  Surface energy
  Surface structure
  Restructuring
Real surfaces
  Contaminants
  Functional groups
  Deformation
Mechanical properties
  Roughness topography
  Defects
Electronic properties
  DoS
Optical

## Slide 3: What is surface? In ideal cases:
Surfaces are defined by ‘relaxed’ atoms (i.e. not constrained in 3D as their internal counterparts are). Dangling bonds from these surface atoms are free to react.
Relaxation and reconstruction are strongly influenced by the bonding type in the bulk material (i.e. metallic, covalent, ionic, and vander waals)
Relaxation of surface atoms leads to reconstruction (rearrangement of atoms near the surface).
(110) Surface of GaAs. Surface atoms (blue) are ‘relaxed’ (i.e. not constrained in 3D).
https://player.slideplayer.com/21/6278052/data/images/img0.jpg

## Slide 4: Miller Index
Wikipedia

## Slide 5
γ surface tension = dW work needed to form surface dA
In thermodynamic equilibrium:
Surface energy

## Slide 6: Surface atoms and defects
Science 18 Apr 1997: Vol. 276, Issue 5311, pp. 377-383 DOI: 10.1126/science.276.5311.377

## Slide 8: Relaxation and Reconstruction
Surfaces are not formed at zero temperature : Heat leads to atomic re-arrangement.
Atoms at a surface have a lower co-ordination than those in the bulk – the origin of surface tension (strictly surface stress in a solid)

## Slide 9: Example Si (100)

## Slide 10: Example Si (100)

## Slide 11: An STM image of the Si(100)-2x1 reconstruction

## Slide 13: Au surface reconstruction

## Slide 14: Modelling of surface electron density
Science Advances 22 Sep 2017: Vol. 3, no. 9, eaao0362 DOI: 10.1126/sciadv.aao0362
Surface electron density on CeCoIn5.

## Slide 15: Surface energy

## Slide 16: Surface energy - milled index
= 4.0
= 3.54
= 3.46

## Slide 17: Contact angle
Young equation
S solid
L liquid
G gas
Spreading parameter S
Complete wetting when S ≈ 0
non-wetting when S ≈ -2 ΥLG
Notes: A direct measure of surface energy can be found by wettability or contact angle.
Youngs eq where each gama is interfacial energy. Gamma SG is interfacial energy between solid and gas.
High energy substrates are much easy to wet than low energy ones.
Also wetting increases if solid surface energy is higher than liquid surface energy.
Direct correlation to cleaning, solvents and how dry a surface stays.

## Slide 18: Surface Electronic States
<
<

## Slide 19
10.3390/nano10020362

## Slide 20: Surface passivation
Dr. Keith T. Butler Department of Chemistry k.t.butler@bath.ac.uk

## Slide 21: Clean surface (0001) of MoS2
DOI: 10.1021/acsami.5b01778 ACS Appl. Mater. Interfaces 2015, 7, 11921−11929

## Slide 22: Clean surface (0001) of MoS2with defects
DOI: 10.1021/acsami.5b01778 ACS Appl. Mater. Interfaces 2015, 7, 11921−11929
defects

## Slide 23: Clean surface (0001) of MoS2 with defects

## Slide 24: Clean surface (0001) of MoS2 with its impurities
Inductively Coupled Plasma Mass Spectrometer

## Slide 25: Surface contamination
5 major contaminant classes (in CMOS processes)
Particles
Metallic ions
Chemicals
Bacteria
Airborne molecular contaminats

## Slide 26: Optical properties of real thin films
1 June 2002 / Vol. 41, No. 16 / APPLIED OPTICS

## Slide 27: Transparent – semi transparent
Photovoltage
Controlled emission
Decoration

## Slide 28: TCO (transparent conductive oxides ) films
ITO Indium Sn oxide
IMO Indium Mo oxide
ITiO Indium Ti oxide
FTO Tin oxide + fluorine
https://doi.org/10.1016/j.tsf.2009.09.044
https://doi.org/10.1515/rams-2018-0006
Resistivity ~10-4 Ωcm or less
Charge carries due to oxygen vacancies
and dopand impurities

## Slide 29: Transparent conductive layer

## Slide 30: Color map L* a* b*
The CIELAB color space (International Commission on Illumination - CIE in 1976)

## Slide 31: Arc deposited Ti-Mg-N Effect of composition
Mg/Ti ratio 0 → 0.53
- colors golden → copper → violet → metallic gray
- conductivity 98 → 457 µΩcm

## Slide 32: Bulk Plasmons
Introduction to Surface Physic, N. Tabet

## Slide 33: Surface plasmos
Introduction to Surface Physic, N. Tabet
https://doi.org/10.1039/C5NR00578G