## Slide 1: Surfaces and Films CHEM E5150 Lecture 2B
J Koskinen

## Slide 2: Items
Low pressure – vacuum
Thin film growth from incoming molecules
Surface characterization

## Slide 3: Items
Low pressure – vacuum
Thin film growth from incoming molecules
Surface characterization

## Slide 4: Vacuum system
VACUUM GAUGE
VACUUM CHAMBER
FLANCE
PUMP
RESUDUAL GAS

## Slide 5: Idea gas collision
Video
https://simplexitysolutions.blogspot.com/2015/
09/interpretation-of-pressure-on-kinetic.html

## Slide 6: Vacuum – low pressure
Prof. K.W. Hipps
www.wsu.edu/~hipps/M571.htm

## Slide 7: Pump-down Pressure vs Time Typical Unbaked Stainless Steel Chamber
Prof. K.W. Hipps
www.wsu.edu/~hipps/M571.htm

## Slide 8: Viscose flow
Viscous flow: λ << D Water in a pipe. The intermolecular interactions are much more important than the interactions with the container.
P ≥ 50 milliTorr = 7 Pa = 5x10-2 Torr
Prof. K.W. Hipps
www.wsu.edu/~hipps/M571.htm

## Slide 9: Knudsen flow
Viscous flow: λ ≈ D Intermediate state. About as many intermolecular collisions as collisons with the wall
Prof. K.W. Hipps
www.wsu.edu/~hipps/M571.htm

## Slide 10: Ballistic flow
Viscous flow: λ ≫ D
Bullets bouncing off walls. Negligible intermolecular interactions. Primary interactions are with the container
P ≤ 0.5 milliTorr = 0.07 Pa = 5x10-4 Torr
Prof. K.W. Hipps
www.wsu.edu/~hipps/M571.htm

## Slide 11: Impingement Rate
Prof. K.W. Hipps
www.wsu.edu/~hipps/M571.htm

## Slide 12: Items
Low pressure – vacuum
Thin film growth from incoming molecules
Surface characterization

## Slide 13: Adsorption of atoms on surface
http://soft-matter.seas.harvard.edu/index.php/File:Fig6.gif

## Slide 14: Thin films growth
J. Vac. Sci. Technol. A 21„5..., SepÕOct 2003

## Slide 15: Nucleation

## Slide 16: Surface diffusion
M. Ohring, Materials Science of thin films, 2002

## Slide 17: Surface diffusion

## Slide 18: Nucleation – minimizing surface energy
ΔW = 2 ⋅ γ ⋅ ΔA = 2 ⋅ γ ⋅ Δx ⋅ b
= 2 ⋅ γ
F = ΔW
b Δx ⋅ b
Force acts tangentially
Tends to decrease surface area
Fundamental to thin film growth:
Surface energy can be minimized by surface diffusion
γ ⋅ A → min
Chemical composition
crystallographic orientation atomic reconstruction
Surface topgraphy
M. Ohring, Materials Science of thin films, 2002

## Slide 19: Nucleation of a growing film
M. Ohring, Materials Science of thin films, 2002

## Slide 20: Density of nuclei
M. Ohring, Materials Science of thin films, 2002

## Slide 21: Coalescence - ripening
M. Ohring, Materials Science of thin films, 2002

## Slide 22: Items
Low pressure – vacuum
Thin film growth from incoming molecules
Surface characterization

## Slide 23: Thin films characterization
Why vacuum for cahracterization of thins film and surfaces?
  Only in high vacuum surfaces are clean
  Many characterization methods are scatter physics:
    Particle in or particle out ( high mean free path λ needed)

## Slide 24: Scattering experiment
IN
OUT
ion, atom, neutron
molecule
electron
photon
particles in vacuum !!
elastic scattering
  mass, density
  diffraction
inelastic scattering
  information on material
    DOS
    bonding
    identification of elements
    …

## Slide 25: XPS -ESCA
wikipedia
Chemical bonding
Composition

## Slide 26: Auger electron spectroscopy
Surface composition
Chemical bond

## Slide 27: LEED Low Energy Electron Diffraction
Crystalline structure

## Slide 28: Seconday ion mass specroscopy

## Slide 29: Seconday ion mass specroscopy
Vacuum roughly 10-6 mbar
Ions: Ar+, O2+, Cs+ (M 133) 1 – 30 keV
sensitivity 1012 – 1016 atoms/cm3
beam focus down to 1 µm
mapping of elements
Depth profiling by sputter etching
seconday ion yield depends on chemical composition of sample
  reference samples with known composition necessary for quantitative analysis
Sputtering - > mixing of composition
  depth resolution decreases when sputtering deeper

## Slide 30: Electron microscopy
Topography
Defects
Impuriteis
Thickness
Atomic structure
Defects

## Slide 31: SEM - EDS Energy Dispersive Spectroscopy

## Slide 32: TEM EELS Electron Loss Spectroscopy
Chemical bonding
Combined with atomic resolution

## Slide 33: Ion beam scatter (Rutherford Back Scattering RBS)
Surface composition
Sample thin film

## Slide 34: Grazing angle x-ray spectroscopy

## Slide 35
X-Ray Reflectivity XRR
Thin Film
  thickness
  density
  roughness
  rougness of interface
Miho Yasaka, The Rigaku Journal, 26(2), 2010

## Slide 36: Thickness of film – contact profilometry
https://australiasurfacemetrologylab.org/new-page

## Slide 37: Optical non-contact profilometry
https://www.laserfocusworld.com/test-measurement

## Slide 38: Residual stress of thin films
R