## Slide 1: Surface preparation
sami.franssila@aalto.fi

## Slide 2: Non-ideal surfaces
Belkind & Gershman; Vacuum Technology and Coatng 2008

## Slide 3: Sources of contamination
Gas phase, e.g. water vapor, ammonia, hydro- carbons.
Airborne particles: pollen, smog, viruses,…
Liquid phase, e.g. dissolved oxygen, dissolved metal ions, waterborne particles, residues of cleaning solvents
Solid phase, e.g. packages and boxes, tweezers, spatulas, conveyor belts, robot hands, chucks and holders,…

## Slide 4: Liquid phase contamination
Water purity (18 MΩ-cm; reverse osmosis)
Cleaning chemicals !!! Never fully pure.
MicroChemical GmbH

## Slide 5
MicroChemical GmbH

## Slide 6: 0.1 ppm sulphate
If we have 2.5 liters of HCl, how many sulphate groups are there ?
2.5 liters is ca. 2.5 kg, or 70 moles ≈ 4*1025 molecules.
0.1 ppm means 10-7  4*1018 molecules.
If we clean a batch of 25 silicon wafers, 100 mm diameter, total surface area is 4000 cm2.
If all sulphate from liquid would be deposited on the wafers, that would equal 1015 molecules/cm2.
Silicon surface atom density is (5*1022 cm-3)2/3 =1015cm-2.

## Slide 7: Solid phase contamination
Objects are stored in boxes, or containers.
Objects are handled by tweezers, hands…
Objects are placed on chucks/holders for processing.
Process chambers are made of solid materials, and the more energetic the process, the more likely it is to kick chamber wall atoms around.

## Slide 8: Avoiding solid contamination
Use inert and hard materials like stainless steel and molybdenum.
Polish surfaces to minimize sites for foreign atom attachment.
Clean tweezers/chucks/chambers/boxes (by wet or dry cleaning, or if really dirty, by mechanical cleaning like sand blasting).

## Slide 9: Surface preparation goals
Removes contamination
Leaves surface in known condition
Eliminates previous step peculiarities
Eliminates waiting time effects

## Slide 10: Surface preparation operations
Cleaning (removal of adherent stuff)
Etching (removal of surface layers)
Activation (surface bond modification)
Passivation (surface bond inactivation)
Deposition (coating the surface)

## Slide 11: Process steps in cleaning
Belkind & Gershman; Vacuum Technology and Coatng 2008

## Slide 12: Cleaning
removal of particles
removal of native films
removal of polymeric films
removal of metals and ions
removal of adsorbed water
https://www.mksinst.com/n/wafer-surface-cleaning

## Slide 13: Surface water
Different kinds of water !
Strongly bonded inner layer (chemisorption, covalent bonds)
Weakly bonded outer layers (physisorption, H-bonds)

## Slide 14: Water removal bake
Water boils at 100oC, in bulk.
But chemisorbed H2O molecules are tightly bound.
Pagliaro: Surface Preparation for Low Temperature CVD Si Epitaxy Processing, https://www.semiconductor-digest.com/2020/02/03/surface-preparation-for-low-temperature-cvd-si-epitaxy-processing/

## Slide 15: Wet cleaning
Aqueous solutions
Acidic solutions
Alkaline solutions
Solvent treatments
immersion
spray/jet

## Slide 16: Ozone-spiked water
Ozone, O3, is very reactive
Ozonated DI-water with 1-100 ppm ozone
Ozone breaks down organic molecules to smaller fragments  water soluble
Ozone addition to acidic cleans is also beneficial.
Abe et al: IEEE TRANSACTIONS ON SEMICONDUCTOR MANUFACTURING, VOL. 16, NO. 3, AUGUST 2003 401

## Slide 17: Ammonia-peroxide (APM)
NH4OH:H2O2:H2O (1:1:5)
a.k.a. APM, RCA-1 and SC-1 (standard clean)
operated at 80oC
removes particles (by undercutting them)
removes organic materials by oxidation
leaves surface hydrophilic (OH-terminated)

## Slide 18: APM reactions
Ammonia peroxide solution works by oxidizing the silicon surface, and subsequently etching the oxide away.
Eq. 12.1 2 H2O2 ==> 2 HO2- + 2H+ peroxide disproportionation
Eq. 12.2 Si + 2 HO2- ==> SiO2 + 2 OH- silicon oxidation
--------------------------------------
Eq. 12.3 Si + 2 H2O2 ==> SiO2 + 2 H2O total reaction for oxidation
Eq. 12.4 SiO2 + OH- ==> HSiO3- (aq) oxide etching
Silicon etch rate in ammonia-peroxide is ca. 0.5 nm/min and typical 10 minute clean thus results in ca. 5 nm silicon etching.

## Slide 19: Detail mechanism of APM
= oxidation + oxide etching
= direct etching of silicon
α is the ratio of the etching reaction of path-1 to total etching reaction.

## Slide 20: Competing etching reactions
etching reaction of a Si substrate proceeds along two paths (path-1, path-2) in APM.
In path-1, the Si surface is oxidized by OH2-
then the SiO2 layer is etched by OH-.
In path-2, the Si surface is directly etched by OH-.
Path-1 is favorable for APM cleaning because path-2 causes some problems, such as too fast etching, an increase in surface microroughness, and a decrease in particle removal efficiency.
Yamamoto et al: IEEE TRANSACTIONS ON SEMICONDUCTOR MANUFACTURING, VOL. 12, NO. 3, 1999

## Slide 21: Particle removal by etching
Ammonia-peroxide mixture, etching rate: 1.1 nm/min.
Yamamoto et al: IEEE TRANSACTIONS ON SEMICONDUCTOR MANUFACTURING, VOL. 12, NO. 3, 1999

## Slide 22: Zeta-potential (surface charge)
If the surface and the particles have opposite charges, they will repel each other  no particle deposition.
Hattori, T. (ed.): Ultraclean surface processing of silicon wafers,

## Slide 23: Undercut etching
Hattori, T. (ed.): Ultraclean surface processing of silicon wafers,

## Slide 24: Hydrogen chloride-peroxide
HCl:H2O2:H2O (1:1:6)
a.k.a. RCA-2 and SC-2
operated at 80oC
removes metal contamination
leaves surface hydrophilic (H & F-terminated)
Hattori, T. (ed.): Ultraclean surface processing of silicon wafers,

## Slide 25: Sulphuric acid
H2SO4 is a strong oxidant
Organics removal by oxidation
Metals dissolved
Oxidation is enhanced by addition of peroxide H2O2
120oC operating temperature
May leave sulphur residue
Chemical waste

## Slide 26: HF, hydrofluoric acid
removes SiO2
comes in many concentrations and formulations:
  DHF (dilute HF), HF:H2O (1:100-1:1000) (room temp)
  BHF (buffered HF, HF:NH4F 6:1 volume ratio (at 35oC)
  strong HF (49%) (room temperature)
leaves surface hydrophobic
does not give a burning sensation immediately
delayed attack on bone after diffusing through the skin
special gel treatment ! Check this gel before using HF.

## Slide 27: Jet cleaning/aerosol cleaning
Kohli & Mittal: Developments in Surface Contamination and Cleaning, Volume 10
Provides mechanical extra energy.

## Slide 28: Dry cleaning
Vapors anhydrous HF
Gases O3, H2, HCl
Ions Ar+
Atoms Si
Photons UV (with Cl2 or O3)
Plasmas CF4
Aerosols CO2
Thermal bake

## Slide 29: Plasma cleaning mechanisms

## Slide 30: Ozone dry cleaning
https://www.mksinst.com/c/wafer-and-chamber-cleaning
Downstream plasma cleaner:
ozone diffuses; no UV-exposure
UV-ozone cleaning:
Combined effect of UV-induced bond breakage and chemical action by ozone
Surfaces will be oxidized in the process (a few nanometers)

## Slide 31: In-situ cleaning in sputtering
Adel et al: Modeling of magnetic properties of iron thin films deposited by RF magnetron sputtering using Preisach model, 2016
Sputter clean the target, while substrate is covered by shutter
Apply bias to substrate, and argon ions will bombard the substrate, and hit off surface specie

## Slide 32: Plasma: sales talk
✓ Cleans even in the smallest cracks and gaps ✓ Cleans all component surfaces in one work step, including the interior of hollow bodies ✓ Residue-free removal of breakdown products by vacuum extraction ✓ No damage to solvent-sensitive surfaces by chemical cleaning agents
✓ Removal also of molecularly fine residues ✓ Fit for immediate further processing. No venting or removal of solvents ✓ No storage and disposal of hazardous, polluting and harmful cleaning agents ✓ Very low process costs
https://www.plasma.com/en/cleaning-with-plasma/

## Slide 33: Etching
Etch away any unwanted film/material
Remove uppermost layers of material itself to reveal hopefully intact material
Etch and undercut particles  particle removal

## Slide 34: Etching easily roughens surface
Polypropylene was simultaneously roughened and fluorinated by etching in argon + PTFE plasma.
Surface is roughened due to the differential rates of crystalline and amorphous regimes.
Reaction time can be used to control the nature of the surface roughness.
Youngblood & McCarthy: Macromolecules 1999, 32, 6800-6806

## Slide 35: Rough on purpose
You might want to increase surface area  keep etching…
Trap light by forward scattering in solar cells and photodetectors.
More area for sensing molecules to attach to.
Improved adhesion by increasing mechanical locking.
Gimple et al: Study on contact materials for sulfur hyperdoped Black Silicon, 2011

## Slide 36: Activation
Provide surface with bonds that are useful in the next step
Chemical treatment, e.g. NaOH  hydroxyl-terminated surface
Physical treatment, e.g. UV, ion bombardment  broken, active bonds
Biological treatment, e.g. single strand DNA attached, to bind to complementary strand

## Slide 37: PDMS in O2 plasma
Native PDMS surface with methyl groups (CH3).
Oxygen plasma treated hydrophilic PDMS surface with hydroxyl and methyl groups.
OH- groups good for bonding with glass/oxides.

## Slide 38: Activation can lower bonding temperature
Reactive bonds from activation enable bonding at lower temperature.
One or both wafers may need to be activated.
At least we need to start from known condition.
Pasternak et al: RSC Adv., 2018, 8, 2161-2172

## Slide 39: Deposition
Adding material on surface
Molecular layers with desired physical properties, e.g. HMDS renders surface mildly hydrophobic  better interaction with hydrophobic material
Self-assembled monolayers, SAMs
Oxidation to create native oxide film
Deposition of real thin films (PVD, CVD, ALD)

## Slide 40: HMDS hydrophobization
Hexamethyl disilazane (HMDS) vapor phase coating renders silicon surface slightly hydrophobic, CA ca. 70o. Hydrophobic polymer in next step will adhere to it better than to oxidized surface with CA ca. 20o.

## Slide 41: SAMs: self-assembled monolayers
A single reaction.
Covalent bond.
Self-terminating.
In liquid or vapor phase.
Slow reaction, hours typically.
Shorter chain  easy assembly
Longer chain  more difficult assembly, but functional group further from surface and effect greater.
time

## Slide 42: SAM functionalities
Hydrophobic fluorinated surface
Hydrophilic, with polar hydroxyl-groups (OH)
Other functionalities

## Slide 43: Perfluorinated surface
Fluorinated surface the most hydrophobic.
Au-S bond (thiol-bond) is very strong (otherwise gold does not readily react; that is why noble metals are called noble)
Linker molecule affects distance of functional group from surface, and coating perfection.

## Slide 44: How to make a surface charged
Example 1: Self-assembled monolayers (SAM) on gold
  Thiol –SH makes a covalent bond to Au
  Amino –NH2 becomes positively charged –NH3+ under acidic conditions
Au
Aminoalkanethiols
Au
Example 2: Silane chemistry on silica, glass, Si-wafer

## Slide 45: Native oxides
Native oxides, e.g. SiO2, TiO2, CuO form in room air, self-limited to ~ a few nm
Thin oxides of slightly better quality can be made by e.g. acid treatment, boiling HNO3 + Si  SiO2 film 2-3 nm
Oxygen plasma and ozone obviously can be used, too

## Slide 46: Native oxides are thin !
W. Henrion et al. / Applied Surface Science 202 (2002) 199–205

## Slide 47: Passivation
Surface specie chosen to be inactive
Just the outermost atoms sometimes enough
Sometimes native oxide works
Sometimes monomolecular layer enough
But you may need to coat the surface for real

## Slide 48: Passivation delays native oxide
W. Henrion et al. / Applied Surface Science 202 (2002) 199–205
”To prepare
atomically flat H-terminated surfaces the samples
were reoxidized in deionized water of 18 Mohm-cm resistivity
at 80oC for 60 min. Afterwards the wafers were placed into NH4F solution for 6.5 min. To minimize dissolved oxygen, the NH4F solution was bubbled by
nitrogen and the preparation was carried out under dry
N2-atmosphere.”

## Slide 49: Aluminum plasma etching
Done in vacuum
2 Al + 3Cl2  2 AlCl3 (moderately volatile product)
After etching, in room air, residues of AlCl3 react with atmospheric water vapor:
AlCl3 + xH2O  Al + yHCl + zH2O
But: 2Al + 6HCl  2 AlCl3 + 3 H2
This is wet etching reaction of aluminum

## Slide 50: Aluminum plasma etching
Solution 1:
After etching in vacuum, we passivate the surface before atmospheric exposure
Oxygen plasma  Al2O3 formed
Then take wafer out of the reactor
Solution 2:
Immediately after taking away from vacuum, wash vigorously in water to remove all AlCl3

## Slide 51: Rinsing and drying are essential
Polyallylamine (PA) film was prepared as follows:
glass slide was rinsed three times with DI water,
soaked in 70% ethanol for 15 min,
rinsed three times with DI water.
Subsequently,
the glass was immersed in 6 M nitric acid for 20 min,
then thoroughly rinsed in DI water.
the glass was then exposed to oxygen plasma,
treated with pure GOPTS at 37 °C for 60 min,
then with 15% PA in water (pH = 11) and left to react at 75 °C for 36 h in a closed container.
Subsequently, the films were
rinsed with DI water (10 times) to remove unattached polymer
dried with nitrogen
This is an antiviral coating.
ACS Appl. Mater. Interfaces 2020, 12, 31, 34723–34727

## Slide 52: COVID-19 resistant surface
The Cu2O/PU coating was fabricated as follows.
A very thin layer of PU was applied to a glass slide using a sponge and then left to dry for approximately 8 min to allow partial curing of the polymer.
Cu2O (10%) in ethanol suspension was sonicated for 3 min, and then, 1 mL was applied to the PU film and left to partially dry for about 5 min at room temperature.
The film was then heated in an oven at 120 °C for 2 h to finish the cure, forcefully blown with compressed nitrogen gas, washed thoroughly with DI water, and dried with a stream of nitrogen gas.
Each piece was then cleaned with argon plasma to remove excess polyurethane.
After plasma cleaning, the film was wetted by water, but the advancing water contact angle was recovered after 1 day.
ACS Appl. Mater. Interfaces 2020, 12, 31, 34723–34727