## Slide 1: Multilayers and interfaces
sami.franssila@aalto.fi

## Slide 2: Why multilayers ?
More functionality and performance
Single layer ARC vs. λ/4 filter
Grain size and orientation are affected by underlayer
More reliability
If aluminum broken because of electromigration, but TiN conducts still
Adhesion layers & barriers
SiOx/SiNx passivation: films complement each other
More process robustness
Etch stop layer, no timed etching needed
TiN on Al reduces reflectivity and eases lithography

## Slide 3: Why not multilayers ?
More complex deposition equipment needed
e.g. Multiple targets, multiple chambers
Deposition thruput compromised
esp. if thickness or nature of films very different
Each new interface is a potential problem

## Slide 4: This lecture deals with phenomena during processing
substrate
thin film 1
thin film 2
surface
interface 2
interface 1
thin film 1

## Slide 5: Magnetic multilayers
1 nm CoFe
2.6 nm Cu
2.5 nm CoFe
0.8 nm Ru
2 nm CoFe
substrate
5 nm Ta
15 nm PtMn
5 nm NiFe
5 nm Ta
Surface roughness must not increase with each successive layer !! Otherwise deposition of extremely thin films becomes impossible.

## Slide 6: Multiple junction solar cell
Poortmans: Thin Film Solar Cells, p. 214
Si:Ge ratio modifies bandgap

## Slide 7: Substrate surface
substrate
Adsorbed water
Carbon & other impurities
Particles
Roughness
Crystal structure
Crystalline defects
Dangling bonds

## Slide 8: Surface reactions
substrate
thin film
Native oxide formation e.g.
Si, Ti, Cu, Cr
But CrO is conductive, others insulators.
Nitridation:
difficult, needs either
  -ammonia exposure
  -high temperature
TiN formation is an exception

## Slide 9: Ambient gases into film
substrate
thin film
Oxygen:
stoichiometry finetuning: Ta2O5
Water:
-into pores
-into PSG (hygroscopic film)
Nitrogen:
Grain boundary stuffing, TiW:N, W:N
Hydrogen (N2:H2 in practice)
Dangling bond passivation

## Slide 10: PSG
CVD oxides have unfortunately many names:
USG = undoped silica glass (=CVD SiOx, x ≈2)
PSG = phosphorous doped silica glass (=CVD oxide, which had P2O5 flow during deposition  phosphorous incorporated into film)
PSG typical: 5 wt% phosphorous
excellent gettering agent for Na+ ions
hygroscopic if too much P
Note: in metals and oxides: 1-5% dopant/alloying element
in semiconducotrs parts per million (10-6) dopant

## Slide 11: Interfaces
Stability of interface in subsequent processing and during use ?
Barrier layers: extra films to stabilize interfaces

## Slide 12: Al-Si phase diagram
A little silicon is soluble in aluminum at 400oC, ca. 0.3 at%
 Al to Si interface is unstable at 400oC

## Slide 13: Junction pitting
Silicon dissolves into aluminum
Aluminum diffuses into silicon via the vacancies left by removed silicon
If aluminum diffusion deep, it will extend to pn-junction
 No pn-junction anymore
Ohring
p
n
junction

## Slide 14: Interface stability: ΔG
Change in Gibbs free energy is given by:
G positive = stable pair; G negative = films react
For reaction titanium reaction with silicon dioxide:
Ti + SiO2  TiO2 + Si
G = GTiO2 - GSiO2 = (160 – 165) Kcal = -5 Kcal, indicative that the reaction can take place.
For Co + SiO2  CoSi2 + Si G> 0, no reaction.

## Slide 15: Reaction Co+Si
Murarka
At high enough temperature the native oxide breaks down, and Co+Si reaction can take place.
SiO2 native oxide delays reaction
Co + Si  CoSi
CoSi + Si  CoSi2 at higher temperature

## Slide 16
Nickel silicide formation
It is not always the case that the silicide that will form is the technologically interesting one !
NiSi is the desired low resistivity material;
NiSi2 is the stable phase that tends to form.
Ohring

## Slide 17: From substrate into film
substrate
thin film
Steel substrates are a source of metals
Glass substrates are sources of sodium
Polymer substrates are permeable to water vapor and oxygen
 Need barrier(s)
substrate
thin film
barrier

## Slide 18: Barriers
substrate
thin film
Atom barrier: blocks atom movements.
Ion barrier: blocks ions.
Total barrier: no atoms, no electrons pass thru.
Barrier can simultaneously act as smoothing layer. This is important if e.g. stainless steel is used.
Spin-on glasses !

## Slide 19: Examples of barriers
Diffusion barrier: <Si>/TiW/Al in IC metallization
Improved diffusion barrier, stuffing: <Si>/TiW:N/Al
Dielectric barrier: SiO2/SiNx/Cu
Ion barrier: glass/Al2O3/ZnS in electroluminescent displays

## Slide 20: Solder joint
Ohring
Pb-Sn will react with aluminum, therefore a barrier (Cr/Cu/Au) is needed.
The alternative strategy of lower temperature does not work because solder has to flow.
Circuit board side
Integrated circuit side

## Slide 21: Stability of metallization
Ti barrier
Ti/TiN barrier

## Slide 22: Alloying effect
Zirconium at grain boundaries acts as an extra barrier, preventing formation of high resistivity Cu3Si

## Slide 23: Copper for IC metallization
General:
low variation
low particle generation
large process window
Barrier:
t < 10 nm thick
ρ < 500 µΩ-cm
Cl conc. < 2%
unif. < 2%
step coverage >90%
rate > 3 nm/min
Low-k:
CMP compatible
Tdepo < 400oC
adhesion on etch stopper
Copper seed
t > 2 nm
unif. < 2%
step coverage ~100%
rate > 10 nm/min
growth and adhesion on etch stopper
Etch stopper:
growth and adhesion
on dielectric
growth and adhesion
on barrier

## Slide 24: Inert annealing changes in film
substrate
thin film
Crystallization
Grain growth
Bond formation: e.g. Si-N bonds formed in PECVD nitride

## Slide 25: Annealing: bond formation
2nd ramp down

## Slide 26: Film poisoning during 2nd deposition
If film 1 is porous or incompletely reacted, it can release atoms and poison film 2.
e.g. film 1 is spin-on-glass, and oxygen or water vapor from it penetrate into aluminum, leading to increased resistivity (and in extreme case, Al2O3 formation).

## Slide 27: Film-to-film modification
During annealing atoms from one film move to the other.
e.g. Film-2 is phosporous-doped oxide, and film-1 is polysilicon, then polysilicon will be doped n-type by phosphorous.
e.g. Film-2 is PECVD nitride, film-1 is a-Si or poly, then during annealing hydrogen from nitride will passivate dangling bonds in silicon.

## Slide 28: Substrate oxidation
substrate
thin film
If thin film precursor is oxygen or water vapor, silicon is easily oxidized, e.g. ALD ZrO2 with O2 pulses.
SiO2 ca. 2 nm

## Slide 29: Annealing: chemical reactions
<Si>
Ti
N2
heat
Surface reaction:
Titanium nitride formation
2Ti + N2  2 TiN
Interface reaction:
Titanium silicide formation
Si + 2 Ti  TiSi2
Solution: anneal in argon

## Slide 30: Annealing: chemical reactions
Cu + Si  CuSix
CuSix is a high resistivity material
Annealing atmosphere:
Even tiny oxygen contamination will lead to copper surface oxidation.
CuOx
CuSix

## Slide 31: Precipitates
Pure Al yield strength 95 MPa
Al-1%Ti yield strength 175 MPa
Al3Ti precipitates formed during 550oC anneal.
Al3Ti has an elastic modulus of 210 GPa, is much stiffer than pure Al (60 GPa).
Stiff precipitates block dislocation movement
through a soft matrix and thereby increase the yield strength.
One can improve the strength of an Al membrane while only slightly diminishing
its conductivity.
10 nm Ti/500 nm Al,
Annealed 550oC, 1 h in N2
Arrows indicate Al3Ti precipitates
Lee, Appl. Phys. Lett., Vol. 76, p. 3415

## Slide 32: Volume changes
In silicide formation, negative volume change  tensile stress
In thermal oxidation, positive volume change  compressive stress

## Slide 33: Annealing multilayers
Top surface reaction
-e.g. oxidation
Film-film reaction
-e.g. Ti + 3Al  TiAl3
Film-substrate reaction
-e.g. Ti + 2Si  TiSi2

## Slide 34: Texture inheritance
Film 2 will register the crystal structure of film 1.
Choosing film 1 to be either amorphous (like SiO2) or polycrystalline (like TiW), will result in different film2 texture and properties.
Molybdenum as film2:
Mo thickness Film 1 Film 2 resistivity
300 nm SiO2 12 µOhm-cm
300 nm TiW 9 µOhm-cm

## Slide 35: Texture inheritance (2)
NiFe soft magnetic underlayer, 80 nm
Ta/Ru intermediate layer, 8/60 nm
CoCrPt:SiO2 recording layer 15 nm nmnm
Protective coating, DLC, 5 nm
Disk substrate (glass or Al-Mg)
Ti (or Ta) adhesion layer, 10 nm
Ta/Ru film will induce suitable crystallinity in the magnetic data storage layer CoCrPt:SiO2
Terminology: CoCrPt:SiO2 means that CoCrPt films contains small SiO2 crystals.

## Slide 36: Symmetric 3-layer
PSG
Poly
PSG
<Si>
Poly will be doped by PSG (phosphorous doped silica glass) symmetrically.
<Si>
<Si>
Au/<Si>/Au mirror planarity assured by a symmetric metallization.

## Slide 37: Acoustic λ/4 multilayers
Al (300 nm)
Mo (50 nm)
ZnO (2300 nm)
Au (200 nm)
Ni (50 nm)
SiO2 (1580 nm)
W (1350 nm)
TiW (30 nm)
SiO2 (1580 nm)
W (1350 nm)
TiW (30 nm)
glass wafer

## Slide 38: Stress evolution
King Tu, p. 131
Much more extensive relaxation takes place in the Al thin films than in bulk.
Thin film grain size, typically ~1 µm vs. ~ 100 µm for bulk, would enable much more extensive grain boundary sliding and hence greater stress relaxation.
Hoo-Jeong Lee,a) Guido Cornella, and John C. Bravman: Appl. Phys. Lett., Vol. 76, p. 3415

## Slide 39: Stress relaxation (1)
King Tu, p. 133

## Slide 40: Hillock generation
Compressive stress is relieved by hillock growth.
If surface is free (as in high vacuum), the surface acts as a sink for vacancies and extra atoms are uniformly distributed over the surface.
Oxide covered surface breaks randomly and hillocks are formed.
Hillocks are same size as microlithographic structures and film thicknesses.
 Hillocks can short two neighboring lines or two films.

## Slide 41: Grain growth
Grain boundaries important because they:
  -act as nucleation sites for growth of new phases
  -act as sites of enhanced reaction rates
  -act as fast diffusion paths
  -act as precipitation sites
King Tu, p. 193

## Slide 42: Grain boundary vs. bulk diffusion
Murarka p. 93
Grain boundaries and dislocations are paths of rapid diffusion (below 0.65 Tm).
Impurities and dopants are easily trapped and precipitated at defects and grain boundaries  fast diffusion paths blocked  improved resistance against processes that rely on them.

## Slide 43: Stress voiding
Murarka p. 84
Grain boundary diffusion vs. bulk diffusion
In order to relieve stress, vacancies diffuse.

## Slide 44: Bamboo structure
Murarka p. 99
3-grain boundaries, active processes during anneal
No 3-grain boundaries  fewer processes at GBs

## Slide 45: Electromigration
King Tu, p. 240
Electron collisions move atoms. Voids formed.
Happens when current density is high.

## Slide 46: Mean time to failure (MTF) due to electromigration
where A is a constant dependent on wire geometry and metal microstructure, J is the current density and Ea the activation energy. The factor n is not known very accurately, but n=1.7 is used for aluminum. For aluminum thin films Ea is of the order of 0.5-0.8 eV, whereas for bulk aluminum it is 1.4-1.5 eV. As a general trend the higher the activation energy, the better the electromigration resistance .

## Slide 47: Alloying to prevent EM
Mean time to failure of 2.5 µm wide lines
pure Al,
Al (0.5 wt % Cu)
Al (2 wt% Cu)
at different temperatures with
1 MA/cm2 current density
Hu, C.-K. et al: Electromigration of Al(Cu) two-level structures: effect of Cu kinetics of damage formation, J.Appl.Phys. 74 (1993), p. 969
500 K = 227oC

## Slide 48: Incubation time
Incubation time before resistance increase sets in (measured at 255C)
Hu, C.-K. et al: Electromigration and stress-induced voiding in fine Al- and Al-alloy thin- film lines, IBM J.Res.Dev. 39 (1995), p. 465

## Slide 49: Dielectric mirrors, enhanced metal mirrors
SH(LH)n =
substrate, high refractive index film,
low+high film stack of n-layer pairs
nHtH = λ/4 condition for thicknesses
Substrate
Film H
Film L
Film H
Film L
Film H
Martin p. 303

## Slide 50: Enhanced aluminum mirror
Martin p. 301
SM(LH)2 design
Glass/Aluminum/SiO2/Ta2O5/SiO2/Ta2O5
510 nm centre wavelength