## Slide 1: Epitaxy, superlattices, nanolaminates

## Slide 2: Epitaxy: single crystalline film on single crystalline substrate
Aluminum on spinel
CdTe on GaAs.
Stacking faults are arranged at regular intervals at the interface and epilayer is perfect

## Slide 3: Homoepitaxy: crystalline film A on top a crystalline wafer A
Single crystal wafer
Epitaxial layer of the same material deposited on top

## Slide 4: Why indeed ?
Epilayer doping concentration different from starting wafer.
Epilayer dopant type different from substrate (n/p –type)
No radial doping profile (as in CZ-crystal pulling)
No vertical doping variation (as along CZ-crystal)
No oxygen (10-15 ppma in CZ-silicon)
No carbon (which comes from SiC and C in CZ)

## Slide 5: Epi requirements
Clean surface
Matching lattices
Small enough CTE difference

## Slide 6: Polycrystalline vs. epitaxial
Crystallites easily seen
Perfectly crystalline film with no grains visible
Yamazaki et al: J. Electrochem. Soc., Vol. 139, No. 4, April 1992

## Slide 7: Epitaxy failure
Lattices do not match
Interfacial contamination
Lattice constant difference
May work if lattice constants integer multiples !

## Slide 8: Lattice mismatch
In homoepitaxy film and substrate lattices are almost identical (because dopants change lattice constants slightly)
In heteroepitaxy lattice mismatch has to be small enough:
η = (af – as)/as where a is lattice constant
Higher the mismatch η , the larger the film-substrate potential W must be

## Slide 9: Strained & relaxed
Misfit dislocations generated at interface
Strained epi-layer

## Slide 10: Strained & relaxed (2)
Relaxed, with defects confined to interface (but it does not always work that way)
Strained,
but with limited epi layer thickness

## Slide 11: CVD epitaxy of silicon
SiH4 (g) ==> Si (s) + 2 H2 (g) T = 1100oC
SiH2Cl2 (g) ==> Si (s) + 2 HCl (g) T = 1150oC
SiCl4 (g) + 2 H2 (g) <==> Si (s) + 4 HCl (g) T = 1200oC

## Slide 12: Rate
mass transport limited
surface reaction limited.

## Slide 13: Miscut & off-orientation
Miscut relative to wafer surface
Off-orientation relative to wafer flat.
https://www.virginiasemi.com/?cont_uid=49
Penanen et al: Phys Rev B DOI: 10.1103/PhysRevB.62.9621

## Slide 14: CVD epitaxy
diffusion to surface
dissociation
desorption of reaction products
diffusion to
main flow

## Slide 15: Major factors affecting film structure
Deposition rate
Vacuum level
Substrate temperature
Surface structure and chemistry

## Slide 16: Ex-situ wet cleaning before depo
Yamazaki et al: J. Electrochem. Soc., Vol. 139, No. 4, April 1992

## Slide 17: In-situ H2 cleaning in CVD reactor
Yamazaki et al: J. Electrochem. Soc., Vol. 139, No. 4, April 1992
In-situ cleaning:
SiO2 (s) + H2 (g) <==> SiO (g) + H2O (g)
Deposition:
SiH2Cl2 (g)
 Si (s) + 2 HCl (g)

## Slide 18: In-situ HCl cleaning
Habuka et al: Journal of Crystal Growth 186 (1998) 104Ð112
HF wet cleaning removes native oxide, by diffusing thru discontinuous organic film.
HCl etches organic material away.
Only then can epitaxial film deposition begin.

## Slide 19: Interfacial contamination
Yamazaki et al: J. Electrochem. Soc., Vol. 139, No. 4, April 1992
SIMS analysis

## Slide 20: Growth vs. etching
SiH2Cl2 (g) <==> Si (s) + 2 HCl (g),
SiCl4 (g) + Si (s) <==> 2 SiCl2 (g)
Etching regime
Deposition regime

## Slide 21: Epi vs. poly
High growth rate results in polycrystalline material: the arriving atoms do not have enough time to find energetically favourable positions before the next layer of atoms arrive.

## Slide 22: Doping in epitaxy
Arsenic is a big atom  lattice under compressive stress
Boron is a small atoms  lattice under tensile stress
Too high doping leads to relaxation.
SiH4 (g)  Si (s) + 2 H2 (g)
2PH3 (g)  2P (s) + 3H2 (g)
B2H6 (g)  2 B (s) + 3 H2 (g)

## Slide 23: Hig boron concentration  stress & dislocations
1 mΩ-cm resistivity corresponds to
1*1020 cm-3

## Slide 24: Germanium-compensation
Small boron
Big arsenic and germanium
Germanium compensates for volume changes and stresses due to small boron atoms.
Why Ge and not As?
Wafer bow,
µm
10 µm
Lattice distortion

## Slide 25: Germanium atom distance ?
6*1020 cm-3 Ge
5*1022 cm-3 Si
Ca. 1% Ge
~5*5*5 silicon atoms for each Ge atom.

## Slide 26: Transition width
But if epilayer is more highly doped, dopants will diffuse into substrate.
Because epitaxy is a high temperature process, diffusion is bound to happen.
If substrate doping higher  dopants will diffuse into epi-layer

## Slide 27: Layer thickness and interface abruptness
p+ wafer, 300 µm
n+ epilayer, 6 µm
n- epilayer, 45 µm
a
15 nm
10 nm
10 nm
10 nm
50 nm
10 nm
500 µm
Si wafer 500 µm
Si85Ge15
Si90Ge10
Si
epi-layers
b
Thick homoepitaxial silicon layers for IGBT power transistor;
Thin heteroepitaxial Si1-xGex layers for high speed bipolar transistors. The hatched layers are graded epi layers with constantly changing germanium content.

## Slide 28: Characterization
    Visual inspection on all wafers.
    Resistivity measurement from a test wafer using either a 4-point probe (n/P and p/N -structures) or CV (p/P and n/N). Destructive methods!
    Thickness measurement optically with an FTIR from a p/P+ or n/N+ -structure. Nondestructive!
    Transition width using SRP.
    Automated inspection for particles, surface defects of all SSP wafers.
    Other measurements as required.

## Slide 29: Selective epitaxy
Si
ox
ox
SEG
ELO
ox
Si
SEG:
Selective Epitaxial Growth
ELO:
Epitaxial Lateral Overgrowth
What happens at the seam ?

## Slide 30: Epi applications: electronics
P- substrate
1-2 µm P-type epi
CMOS:
p-type epi on a P- substrate.
Produces COP-free surface.
Thickness and resistivity uniformity specifications not critical.
Power devices:
Highly doped substrate reduces resistive losses, but devices need to be made in lightly doped material.

## Slide 31: Epi applications: MEMS
n- epi
p-Si
Membrane thickness control in MEMS: electrochemical etch stop
p++ epi
p-Si
P++ etch stop: when boron concentration exceeds 5*1019 cm-3, KOH etching slows down

## Slide 32: Heteroepitaxy: crystalline film A on top a crystalline wafer B
Multiple layers of single crystal AlAs and GaAs grown on top of single crystal GaAs wafer

## Slide 33: Multilayer hetero-epitaxy
Borschel, C. et al: Structure and defects of epitaxial Si (111) layers on Y2O3 (111)/Si(111) support systems, J. Vac. Sci. Technol. B 27 (2009) pp. 305-309
Zhang & Jiao: Energy Bandgap Engineering of Transmission-Mode AlGaAs/GaAs Photocathode 2018
If we can grow A on B, we can grow B on A.

## Slide 34: Lattice match requirement
Lattice match difference:
= (a subs – a film)/a subs
GaAs/AlAs 0.2%  small and easy
Si/Ge, 4.17 %  difficult (but not impossible)
Lattice constant

## Slide 35: Hetero-epitaxy GaAs/AlAs
https://www.nature.com/articles/s41598-018-20155-0
AlxGa1-xAs can be grown in any ratio, since lattice matching.

## Slide 36: Thermal expansion
Si 2.6 ppm/oC
Ge ‎5.9 ppm/°C
GaAs 6.8 ppm/oC
AlAs 5.2 ppm/oC
InP 4.6 ppm/°C

## Slide 37: MBE: Molecular Beam Epitaxy
MBE = advanced evaporator
Lynn F. Schneemeyer, in Encyclopedia of Physical Science and Technology (Third Edition), 2003
Effusion cell = Knudsen cell = thermal equilibrium source  stable flux of vapor

## Slide 38: GaAs quantum dot (QD) laser
Liu et al: Quantum dot lasers for silicon photonics, 2015
Grading of Al & Ga concentrations
Be doping
Miscut substrate

## Slide 39: Superlattice and quantum well (SQW/MQW, single/multiple)
Lee et al: Current Applied Physics Volume 17, Issue 3, March 2017, Pages 398-402

## Slide 40: Epitaxy considerations
Thermal mismatch:
CTE differences cause strains
Diffusion:
high T produces surface diffusion which helps epitaxy, but too high T produces diffusion of film atoms into substrate
Usable temperature range e.g. 0.35T – 0.4T
Defects in substrate:
Misfit dislocations can propagate into film
Impurities (from the gas phase):
Can act as faux nucleation sites, prevent surface diffusion, generate defects, cause oxidation (oxygen, water vapor)
Surface impurites (not removed by cleaning):
Native oxides completely prevent epi, and must be in situ removed

## Slide 41: New materials: nanolaminates
Adriana Szeghalmi,Stephan Senz, Mario Bretschneider, Ulrich Gösele, and Mato Knez, APL 2009

## Slide 42: Inorganic-organic NL
Salmi, Ritala, DOI: 10.1002/cvde.200906770
5x(10 nm PI/10nm Ta2O5)/Si.

## Slide 43: Nanolaminate vs. superlattice
Similar layer thicknesses
Similar deposition equipment
But: amorphous or polycrystalline films

## Slide 44: Sputtered NL
This structure repeated 50 times
Bajt, S.: Improved reflectance and stability of Mo-Si multilayers, Opt. Eng. 41(2002), pp.1797–1804.

## Slide 45: NL by ALD
S.M.George et al: Thin Solid Films 515 (2007) 7177–7180
Flexible polymer substrate  folding space mirror for X-ray telescope

## Slide 46: X-ray mirror
S.M.George et al: Thin Solid Films 515 (2007) 7177–7180

## Slide 47: Al2O3/Ta2O5
Szeghalmi & Knez: APPLIED PHYSICS LETTERS 94, 133111 2009

## Slide 48: Ionic conductivity
The 4:1 cycle ratio (10.4 mol% Y dopant) resulted in the highest conductivity of all films, which was 2 orders of magnitude greater than bulk YSZ (8 mol% Y dopant).
Johnson et al: Materials Today Volume 17, Number 5 June 2014

## Slide 49: NLs as vapor barriers
Yoon & Sung: DOI: 10.1021/acsami.6b15404
Multilayer structures are unlikely to have defect in the same position in every layer  improved leak tightness.

## Slide 50: Barrier properties of NL
Peter F. Carcia, Robert S. McLean, Zhigang G. Li, Michael H. Reilly, and Will J. Marshall
Citation: Journal of Vacuum Science & Technology A 30, 041515 (2012); doi: 10.1116/1.4729447
Water vapor transmission rate reduced by 4 orders of magnitude for same thickness.