## Slide 1
Surfaces and Films CHEM-E5150
Tribology
Jari Koskinen

## Slide 2: Tribology
Tribology is
  science and technology of interacting surfaces in relative motion
  origin in the Greek word tribos meaning rubbing
  friction, lubrication, and wear of engineering surfaces
  understanding surface interactions in detail and then prescribing improvements in given applications.

## Slide 3: Practical objectives of tribology
G.W. Stachowiak, A.W. Bachelor, Engineering tribology 3rd edition, 2005

## Slide 4: Operation conditions and type of wear Flowchart
G.W. Stachowiak, A.W. Bachelor, Engineering tribology 3rd edition, 2005

## Slide 5: Materials selection quide for wear control
G.W. Stachowiak, A.W. Bachelor, Engineering tribology 3rd edition, 2005

## Slide 6: Dynamic viscosity

## Slide 7: Dynamic viscosity
“Poise”

## Slide 8: Kinematic viscosity
“Stoke”

## Slide 9: Viscosity-temperature

## Slide 10: Viscosity – temperature of selected oils

## Slide 11: Pressure -Viscosity
https://www.eneos.co.jp/english/company/rd/intro/lubricants/kudokei.html

## Slide 12: Viscosity – shear rate Newtonian fluid

## Slide 13: Elasto hydrodynamic lubrication
ƞ = ƞ0exp(⍺p). (Barus 1893)
ƞ viscosity
ƞ0 viscosity at normal pressure
p pressure
⍺ pressure-viscosity coefficient

## Slide 14: Pressure -Viscosity
https://www.eneos.co.jp/english/company/rd/intro/lubricants/kudokei.html

## Slide 15: Title
Mike Ramsey Noria Corporation 2019

## Slide 16: Viscosity non-Newtonian fluids
Typically colloids, e.g. cornstarch

## Slide 17: Contact mechism
Herzain contact
Contact mechanism Wiki

## Slide 18: Assumptions in Hertzian theory
  The following assumptions are made in determining the solutions of Hertzian contact problems:
  The strains are small and within the elastic limit.
  The surfaces are continuous and non-conforming (implying that the area of contact is much smaller than the characteristic dimensions of the contacting bodies).
  Each body can be considered an elastic half-space.
  The surfaces are frictionless.

## Slide 19: Herzian pressure (sphere on flat)
MAXIMUM PRESSURE:
F
https://media.springernature.com

## Slide 20: Johnson-Kendall-Roberts (JKR) model of elastic contact
incorporate the effect of adhesion in Hertzian contact

## Slide 21: Levels of tribological testing

## Slide 29: Scrach testing - adhesion

## Slide 32: Tribology Testing - Overview
“Simple” system and highly reproducible measurement
Simulate real frictional conditions
  Contact pressure
  Movement mode
  Sliding speed
  Static partner (size, geometry, mechanical properties, etc)
  Lubrication
  Environmental condition (temperature, vacuum, humidity, etc)
Ball/Pin
Disk

## Slide 33: Tribology Testing - Overview

## Slide 34: Tribology Testing - Contact Mechanics Modeling
Modeling software included inside every Anton Paar Tribometer package

## Slide 35: Tribology Testing - Contact Mechanics Modeling
Contact Radius
Mean Contact Pressure
F: normal load, R: ball radius, E*: reduced modulus
0.0
1.0
2.0
3.0
4.0
-2.0
-1.0
0.0
1.0
2.0
0.5
x/a
z/a
Von Mises
iso-stresses
a
y=0
µ=0
max
~ 0.5 a
For coated materials, max Von Mises stress is important
Hertz contact model (ball on flat)

## Slide 36: Tribology Testing - Coefficient of Friction
100Cr6 Steel ball against TiN coated steel

## Slide 37: Tribology Testing - Wear
Wear of Sample
Wear of Ball

## Slide 38: Tribology Testing - Wear
Ball wear volume = Volume of the worn cap
Sample wear volume = Cross section area * wear track circumference
Wear Rate
V: wear volume, F: normal load, l: sliding distance

## Slide 39: High Temperature Tribometer (THT)
THT up to 800°C
THT up to 1000°C
Water chiller included
for all THT

## Slide 40: High Temperature Tribometer (THT)
Double LVDT sensors to cancel thermal drift error
Cylinderical Oven for homogenous sample heating
Water cooling system for efficient temperature control and safe utilization
Double LVDT sensors for Friction Force
Differential measurement by double LVDT sensors to avoid thermal drift on Ft
Elastic Arm
Monolithic machining with extremly high linearity
Sample thermal couple
(for THT 800°C)
Direct contact with the sample for precise temperature measurement
Cylindrical Oven
Homogenous sample heating
Water cooling system
Efficient circulating water cooling system
Certified Weights
Stable normal load application without problem of thermal drift (vs. Servo loop control)

## Slide 41: Nano tribology

## Slide 42: Diamond tip (Berkovich) wear of ALD TiO2 on a silicon substrate
Jussi Lyytinen et al., Volumes 342–343, 15 November 2015, Pages 270-278

## Slide 43: Effect of ALD processing temperature to abrasive nano wear
Jussi Lyytinen et al., Volumes 342–343, 15 November 2015, Pages 270-278