## Slide 1: Fringed fibrillar model

## Slide 2: Longitudinal disorder: semi-crystallinity
Crystallographic data presents evidence
that cellulose within microfibrils is not
totally crystalline.
Proposition:
cellulose runs through alternating
crystalline and “ amorphous” regions.

## Slide 3: Fringed-fibrillar model of CMFs
Hearle 1958
Hess and Kiessig 1953
Dolmetsch 1968
According to various models, disordered cellulose segments
coexists with crystalline cellulose in native cellulose microfibrils.

## Slide 4: Semicrystallinity of microfibrils
Fringed micellar model
Fringed fibrillar model
Mark J. Phys. Chem. 1940, 44, 764.
Hearle J. Polym. Sci. 1958, 28, 432.
Original models were designed for all polymeric fibrils: synthetic, regenerated and native alike

## Slide 5: Synthetic polymers vs. cellulose
Loos et al. Macromolecules 1999, 32, 8910.
Polyethylene
High resolution morphology by AFM
Cellulose microfibrils
isolated from wood pulp
Amorphous segments visible
Amorphous segments NOT visible

## Slide 6: The original fringed fibrillar model
Saito et al. Biomacromolecules 2006, 7, 1687.
Saito et al. Biomacromolecules 2007, 8, 2485.
Fringed fibrillar model
Hearle J. Polym. Sci. 1958, 28, 432.
Modern TEM images of microfibrils isolated by TEMPO-mediated oxidation do not support the Hearle model where fibrils are branched and polydisperse in width

## Slide 7: More realistic picture of a microfibril
“Amorphous” regions are more like defects between the crystallites
Their length is probably very small (maybe 1-2 nm)
Defects: more realistic
Bulky amorphous regions: less realistic

## Slide 8: Implications of fringed-fibrillar model
Page J. Pulp Paper Sci. 1983, 3, TR15.
Alternating crystalline-amorphous regions explain well
the macroscopic mechanical properties of cellulosic materials.
The length and width of the crystalline domains
depend on the native source of the material.
Elastic properties of isolated cellulose
nanofibrils depend on their native source.

## Slide 9: Reservations with fringed fibrillar model
When you see data of the degree of crystallinity or crystallinity index of cellulose, its physical meaning is unclear
If the degree of crystallinity is, e.g., 64%, it does not mean that 64% of the cellulose is crystalline and 36% is ”amorphous”
Probably much of the material responsible for the ”amorphous” response resides on the microfibril surface
Cellulose I and cellulose II degrees of crystallinity should not be compared with each other
Systematic sets of data can be compared with each other if the crystalline forms, the analytical method, and the raw materials are similar