## Slide 1: Levelling-off degree of polymerization (LODP)

## Slide 2: Acid hydrolysis of cellulose
H2O/H+
+
/2
Glucose
Acid hydrolysis involves the breakage of glycosidic bond by addition of water, catalyzed by acid
High concentrations are required for complete degradation (e.g., 72% (w/w) H2SO4)

## Slide 3: Kinetics of acid hydrolysis of cellulose
When milder acid concentrations are used, DP first drops fast, after which it almost halts, hitting the LODP
Traditionally LODP is determined with 2-3 M HCl at around 100ºC
Common explanation for LODP: “amorphous” regions are hydrolysed and crystallites are left intact

## Slide 4: LODP of different cellulose sources
Material | LODP
Wood pulp | 100-250
Cotton linters | 100-250
Ramie | 200-350
Valonia | 7000
Notice the large variation in numbers for the same source

## Slide 5: Molecular weight distribution at LODP
log Mw
Diff log Mw
Hydrolysed 4 h
Hydrolysed 120 h
Cotton linters LODP ~150
Notice: bimodal distribution

## Slide 6: Discrepancies with LODP
Cellulose substrate and reference | LODP | Yield loss (%) | Conditions for determining LODP
Cotton linters | 200-250 | n.a. | 2.5 N HCl, 105ºC, 15 min
Cotton linters | 187 | 7 | 2.5 N H2SO4, 96ºC, 6 h
Cotton linters | 253 | 2 | 2.5 N H2SO4, 100ºC, 30 min
Cotton linters | 190 | 4.4 | 2.4 N HCl, 100ºC, 1 h
Cotton linters | 100 | 6 | 6.5 N HCl, 108ºC
Cotton linters | 200 | 3.5 | 2.5 N HCl, 100ºC, 30 min
Cotton linters | 162 | 5 | 5% HCl, 95ºC, 1 h
No standard method to measure LODP exists
Many different values for similar cellulose grades have been reported
Amount of material lost during hydrolysis (yield loss) also varies a great deal

## Slide 7: Does LODP represent the length of the crystalline region?
Cellobiose length in cellulose I crystal: 1.03 nm
Length calculated from LODP should correspond to crystallite length measured by XRD or NMR

## Slide 8: Crystallite length vs. LODP
Material | LODP | Crystal length by XRD*
Wood pulp | 100-250 | 23 nm
Cotton linters | 100-250 | 35 nm
Crystal length determined from CMFs does not correlate with LODP
Possible reason: diffraction and/or spectroscopy cannot detect the CMF twist and interprets it for a shorter crystallite
* X-ray diffraction

## Slide 9: Careful comparison of LODP and small angle neutron scattering
Nishiyama et al. Biomacromolecules 2003, 4, 1013.
DP of ramie fibres after
HCl hydrolysis
Small angle neutron scattering (SANS)
pattern of untreated ramie
LODP
Crystallite length (i.e. length of crystalline domains) by SANS agrees with the level-off degree of polymerization (LODP).

## Slide 10: Careful comparison of LODP and small angle neutron scattering
Nishiyama et al. Biomacromolecules 2003, 4, 1013.
DP of ramie fibres after
HCl hydrolysis
LODP
The yield loss upon controlled acid hydrolysis is very small (~1%)
This implies a very short disordered region (4-5 anhydroglucose units)
Disordered – not amorphous