## Slide 1: PHYS-E0421 Solid State Physics Period V, spring 2019
Martti Puska
Rina Ibragimova
Hannu-Pekka Komsa
Arsalan Hashemi
Lecture 14, Monday 20.5.2019
Dielectric Properties of Solids
Magnetismivity

## Slide 2: Magnetic properties
The last lecture TODAY
Response of materials to an external magnetic field
  Magnetic quantities, magnetism is quantum mechanics (home work)
  Quantum mechanical description
  Atomic diamagnetism, paramagnetism (lecture work)
  Response of free electron gas
  Spontaneous magnetism (Ferromagnetism and antiferromagnetism)
  Exchange interaction, H2 molecule, Heisenberg spin Hamiltonian
  Mean-field approximation for ferromagnetism of magnetic moments
  Spin waves (low-energy excitations)
  Free electron gas
  Stoner model for ferromagnetism of itinerant electrons
  Antiferromagnetism
  Domain structure

## Slide 3
Ferromagnetism of Localized Moments, Summary
M in different temperature regions:
Mean-Field Theory
Exchange
interaction
Self-consistent
solution
External field

## Slide 4
Ferromagnetism of Localized Moments, Summary
Beyond the Mean-Field Theory, magnons

## Slide 5
Ferromagnetism of Free Electron Gas
(Elliott pp. 607-608)
[E(7.212)]
(Infinite system)
Spin triplet, antisymm. orbital w.f.
Cf. H2
[E(7.211)]
 Applying quantitative band theory
q.e.d.
”Proof”

## Slide 6
Exchange Hole
A pair of electrons
Total electron density around a given electron i
Average densities
Fix the origin at the electron at ri
Probability for another spin-up electron inside dr at r
[~E(7.213)]
[E(7.216)]
Total (spin up + spin down) electron charge density
Insert
Electron density  length scale
Oscillations
Fast decay
Central quantity in electron structure theories

## Slide 7
Exchange Hole
[E(7.216)]
Total (spin up + spin down) electron charge density
Exchange energy
Sum rule
Density-functional theory (DFT)
Exchange-correlation functionals
Atomistic systems
First-principles electronic structure modeling
Hartree-Fock approximation:
Total energy = kinetic(+) + exchange(-) energies
Homogeneous electron gas
See, Ashcroft-Mermin,
Chapter 17 (HF fails for EG)
Additional correlation energy(-)
e- - e- repulsion more accurately
Quantum Monte Carlo

## Slide 8
Ferromagnetism due to itinerant electrons
(Elliott 7.2.5.3)
Exchange interaction
Heisenberg Hamiltonian
Modeling magnetic 4f and 3d impurities
Free electrons
J > 0 (Ferromagnetic)
STONER BAND MODEL
Ferromagnetism of,
e.g., bulk Fe, Co, and Ni
Strong ”Pauli paramagnetism”
with an internal Beff
Densities of states
Spin-up and spin-down densities
Self-consistent
solution
Stoner model


## Slide 9
 Density of states 
Stoner Band Model of Ferromagnetism
(Elliott 7.2.5.3)
DOS(E), Ni
Stabilization of magnetic moment
Exchange interaction lowers the energy levels of spin-up electrons
Spin flips
Kinetic energy increases
Flat d bands 
High DOS(EF)
Small energy increase for a large number of flips
Magnetic moments / atom
Ni: mm = 0.56 mB
Fe: mm = 2.2 mB
Itinerant electrons ”decoupled” from ions
 mm = integer x mB
Quantitative materials parameters
directly related to electron bands
/

## Slide 10
Ferromagnetic materials
Kittel
mm

## Slide 11
Stoner Band Model of Ferromagnetism
 Quantitative criterion for existence of ferromagnetism
Exchange interaction
Lowering of bands is the stronger, the more there are electrons with the same spin
[E(7.239)]
k-independent shifts for bands
Stoner parameter
 Strength of exchange interaction
[~E(7.240)]

## Slide 12
Stoner criterion of ferromagnetism
Dn is not calculated!
The criterion tells, is the spin-
compensated solution stable!
Fermi-Dirac statistics  Occupation of spin-up and spin-down bands  Dn
(c.f. Theory of Pauli paramagnetism)
[~E(7.243, 245)]
Total spin-degenerate DOS
[E(7.246)]
Stoner criterion
Spin-compensated calculation

## Slide 13
Obtained from atomic orbitals
Obtained from spin-compensated band structure calculation
Stoner Criterion

## Slide 14
Stoner criterion fulfilled due to electron confinement
Electron confinement
Flat E(k) bands Large DOS(EF)
Magnetism
Ferromagnetic

Ferromagnetic

Antiferromagnetic

Examples
Pd surfaces (2D) 3) Zigzag graphene nanoribbons (Nature 514, 608 (2014) )
Atomic chains (1D)
Flat bands at Fermi level

## Slide 15
Stoner Model, Temperature Dependence of Magnetization
Ni
Are mean field theory and Stoner model related?
Can we find the same equation to be solved self-consistently?

## Slide 16
Simplified picture around EF
States furher below EF in balance
Stoner Model, Temperature Dependence of Magnetization
(Elliott pp. 618-619)
[E(7.249)]
Two-level model in FD-statistics (EF = 0), T > 0
[E(7.250)]
Why EF=0?
Why still EF=0?

## Slide 17
Stoner Model, Temperature Dependence of Magnetization
As in the mean-field model, but
Mf-model: total S of an ion  M
Stoner model: Dn/atom  M
Ni
Comparison with experiments:
Fe
B0 = 0

## Slide 18
Antiferromagnetism and ferrimagnetism
(Elliott 7.2.5.6)
 Microscopic origin
Exchange parameter Jij < 0
E.g. superexchange 
Examples, Mn, Fe, Co, and Ni –oxides
- band model  metals
- electron-electron correlations (Hubbard model)  insulator, antiferromagnet
Antiferromagnetism
Ferrimagnetism
Examples, Ferrites (metal oxides)
Intertwined ionic and electronic structures:
- Cubic unit cell with metal atoms in 8 tetrahedral (A ) and 16 octahedral (B) sites
- E.g., Magnetite (lodestone) FeO Fe2O3 mixed valence system (Fe2+ , Fe3+ )

## Slide 19
Ferrimagnetism and antiferromagnetism
Example: Ferrimagnetic magnetite (lodestone) FeO Fe2O3
 Microscopic origin
https://www.researchgate.net/publication/227992376_Spin_Structures_and_Spin_Wave_Excitations
Tetrahedral sites,
8 / cube
Octahedral sites,
16 / cube

## Slide 20
Ferrimagnetism and antiferromagnetism
Example: Ferrimagnetic magnetite (lodestone) FeO Fe2O3
 Microscopic origin
Superexchange
via O-ions
Antiferro-
magnetism
Double Exchange:
Electron transfer and
Pauli principle
 Ferromagnetism
8 tetrahedral
sites A
8+8 octahedral sites B
(d-electron levels spitted by
crystal field and exchange interaction)

## Slide 21
Antiferromagnetism
”Frustration”, neutron
diffraction
Example: (Hubbard) insulators Mn, Fe, Co, and Ni –oxides
NaCl –structure, two interpenetrating FCC’s
Metal atoms
MnO
Monatomic BCC, SC structures
No frustration
O atoms
(fill in more)
Compare peak shape changes at ~23o and ~47o  ?
indexes?

## Slide 22
How do you explain the two branches below qN?
Antiferromagnetism
[E(7.279)]
Susceptibility above and below critical temperature, Mean field theory
[E(7.284)]

## Slide 23
Ferromagnetic Domains, why do they exist?
(Elliott 7.2.5.5)

## Slide 24
Ferromagnetic Domains, Domain Walls
Magnetic moments misaligned over domain interfaces
Bloch wall thickness d= ?
180o Bloch walls between domains

## Slide 25
Initial magnetization curve
Ferromagnet in an External Field H, T < qCW
Saturation
Irreversible
Reversible
Barkhausen
noise
Reversible movement
of domain walls
Irreversible
disappearence
of domain walls
HYSTERESIS
Bloch walls sticked when crossing material inhomogenities
Barkhausen jumps
Resistance of saturation

## Slide 26
Ferromagnet in an External Field H, T < qCW , Hysteresis
Saturation
magnetization
Remanent
magnetization
Intrinsic
coersivity
 Irreversible processes
Inhomogeneous material
 Pinning of domain walls
Ideal permanent magnet
Transformer cores
B
H
Ideally:
Homogeneous materials
Freely moving domain
walls
Lamellar structure, high
resistivity
 Eddy current losses

## Slide 27: Magnetic properties
Response of materials to an external magnetic field
  Magnetic quantities, magnetism is quantum mechanics (home work)
  Quantum mechanical description
  Atomic diamagnetism, paramagnetism (lecture work)
  Response of free electron gas
  Spontaneous magnetism (Ferromagnetism and antiferromagnetism)
  Exchange interaction, H2 molecule
  Mean-field approximation for ferromagnetism of magnetic moments
  Spin waves (low-energy excitations)
  Free electron gas
  Stoner model for ferromagnetism of itinerant electrons
  Antiferromagnetism
  Domain structure